GENERAL COMMERCIAL TERMS (GCT)

TECHNISTONE, a.s.

PART III

TECHNICAL MANUAL

INSTALATION, USE AND MAINTENANCE INSTRUCTIONS FOR ENGINEERED STONE

technistone®

FirstNet, JSC

Vodickova 791/41

110 00 Prague 1

Czech Republic

Phone: +420 602 277 500

Fax: 	  +420 224 152 071

e-mail: info@firstnet.cz				    http://technistone.firstnet.cz

Contents

1. Purpose	5

2. Concepts	5

2.1. Concepts	5

2.1.1. Engineered stone	5

2.1.2. Slab	5

2.1.3. Format	5

2.1.4. Final product	5

2.1.5. Surface finish	5

2.1.6. Aesthetic parameters	5

2.1.7. Inert materials	5

3. General product information	5

3.1. Product composition	5

3.2. Description of the production technology	5

3.2.1. Production of the semi-finished product	5

3.2.2. Machining of the semi-finished product	5

3.2.3. Product surface finish	6

3.2.4. Surface specification of the products with the surface finish: semi-gloss, honed, brushed, antique finish and sand-blasted finish	6

3.3. Production groups of the engineered stone Technistone	7

4. Technical parameters of the product	7

4.1. Dimensions of the product	7

4.2. Dimension tolerations of formats	7

4.3. Dimension tolerations of the slab	7

4.4. Basic technical requirements on the physical and mechanical characteristics of the product	8

4.5. Average values of basic physical and mechanical characteristics of the production groups	9

4.6. Other values of the physical and mechanical, chemical, hygienic and fire characteristics of the product	10

4.6.1. Average mass of Technistone products	10

4.6.2. Average density values	11

4.6.3. Strength characteristics	13

4.6.4. Thermal expansion coefficient of the product	18

4.6.5. Dimensional stability of the product	19

4.6.6. Physical tests of surface resistance	20

4.6.7. Thermal resistance of the surface	21

Determination of the heat-shock resistance according to EN 14617-6	28

4.6.8. Antislipperness properties of the product surface	29

4.6.9. Chemical durability of polished and brushed product surface	32

Resistance of the surface of the Technistone product to water and chemical defrosting agents exposure	46

4.6.10. Technical fire characteristics of the product	46

4.6.11. Hygienic properties of the product	46

4.6.12. Frost resistance	47

5. Recommended use of the product	48

5.1. Installation	48

5.1.1. Recommended thickness depending on the dimension of the format (of the standardly loaded area)	48

5.1.2. The influence of the surface finish on the antislipperness properties of the product (installation)	48

5.1.3. Suitability of the usage of the product at higher mechanical load	49

5.1.4. Suitability of the usage of the product at high thermal load	49

5.1.5. Recommended thickness of the format according to the dynamic (travelling) load of the face/true side	49

5.1.6. The recommended use of the individual production groups of the Technistone product and its dependence on the expected abrasive loading of the product	51

5.2. Raised floors	51

5.3. Wall cladding	52

5.4. Stair components	52

5.5. Worktops	52

5.5.1. Recommendation of the usage of individual production groups for the worktops	54

5.5.2. Recommended usage of insulating pads against the thermal shock	54

5.6. Other usage	54

6. Installation of the product	55

6.1. General rules	55

6.2. Installation of floor and wall tiles	56

6.2.1. Recommended adhesives	56

6.2.2. Recommended jointing materials	57

6.2.3. Tools and instruments	57

6.3. Beddings	57

6.3.1. Generally	57

6.3.2. Concrete	58

6.3.3. Usual cement finishes	58

6.3.4. Cement finish Mapecem	58

6.3.5. Cement finish Topcem	58

6.3.6. Previously existing floors and facing	58

6.3.7. Metal	58

6.3.8. Spattered dashes and plasters	58

6.3.9. Walls from blocks of expanded cement	58

6.3.10. Anhydride floors	58

6.4. Levelling of bedding	59

6.5. Environment conditions at the installation	59

6.6. Preparation of adhesives	59

6.7. Application of adhesives	59

6.8. Dilatation and dividing joints	60

6.9. Jointing	61

6.9.1. Cleaning of the floor tiles after finished jointing	61

6.10. Installation of floor tiles on surface with floor heating	61

6.11. Installation of the product at higher thermal load	62

6.12. Installation of the product as stair component	62

6.13. Installation of glued wall tiles	62

7. Maintenance and cleaning of the Technistone product	63

7.1. General information about maintenance and cleaning	63

7.2. Important instructions for cleaning the products	64

7.3. Recommended special agents	64

7.4. Recommended equipment for mechanical curing of the product on floors	67

7.5. Cleaning of the product surface	67

7.5.1. Cleaning of the surface after installation or before the application of protecting wax / impregnation layer	67

7.5.2. Cleaning of the product in households (kitchen countertops, tables..)	67

7.5.3. Special cleaning of the product surface	67

7.6. Protection of the product with polished surface	68

7.6.1. Protection of the product surface on floors with low mechanical and abrasive load	68

7.6.2. Protection of the product surface on floors with higher mechanical and abrasive load	68

7.6.3. Improvement of surface antislipperness finish	68

7.6.4. Regular maintenance of the floor areas with polished surface	68

7.7. Protection of product with semi-gloss, honed surface	68

7.8. Protection of brushed/antique finish or blasted product surface	68

7.8.1. Regular maintenance of floor areas with honed, brushed/antique finish and blasted surface	69

7.9. Protection of surface of furniture components, kitchen countertops, wall cladding	69

7.10. Protection of surface against paints and varnishes	69

7.11. Protection against abrasive mechanical impurities	69

7.12. Renewal of floor tiles (polished surface)	69

8. Other machining of the product	70

8.1. Binding and gluing of the product	70

8.2. Cutting and milling of the product	70

8.3. Drilling of the product	70

8.4. Honing and polishing of the product	70

9. Answers to frequent questions of the customers	71

9.1. What is it Technistone® ?	71

9.2. What is Technistone® made from?	71

9.3. Is Technistone® the same throughout its volume or is its color and structure built only on the surface?	71

9.4. What is the comparison of Technistone® (used e.g. on a kitchen countertop) to natural granite, marble, Corian® or postforming?	71

9.5. How can the individual types of Technistone® be characterized?	71

9.6. Resists the Technistone® surface used on the kitchen countertop mechanical damage?	72

9.7. Resists the surface of the Technistone® product used on the kitchen countertop thermal load?	72

9.8. Is the Technistone® product harmless to health?	72

9.9. Are the chromatic and structural particles taking their part at the appearance of the Technistone® surface intentional?	72

9.10. Is it necessary to take into account the thermal expansion when using the Technistone product as floor and wall tiles?	73

10. Safety regulations for the product	74

10.1. Identification	74

10.2. Composition	74

10.3. Physical Data	74

10.4. Fire Fighting Data	75

10.5. Flammable Properties	75

10.6. Extinguishing Media	75

10.7. Fire Fighting Instruction	75

10.8. Self Ignition Temperature	75

10.9. Stability And Reactivity	75

10.10. Toxicological Properties Of The Made Product	75

10.11. Hazardous Identification During Handling	76

10.11.1. Potential Health Effects	76

10.11.2. Personal Protective Equipment	76

10.11.3. Procedures And Controls	76

10.11.4.	77

10.11.5. First Aid Procedures	78

10.12. Ecological Information	78

10.13. Disposal Consideration	78

10.14. Other Information	78

11. Records	78

12. Related documents	78

12.1. Internal	78

12.2. External	78

# Purpose

The purpose of this instruction is to define the basic technical requirements, suggestions and guidelines related to the introduction of the product, its usage, installation and maintenance.

# Concepts

## Concepts

### Engineered stone

High-quality, imporous, composite material, built-up from hard, inorganic, polishable granulates, compactly bound together with a binder and a filler, colored with various pigments, having a smooth, resistant surface, in a variety of sizes and with a wide range of applications.

### Slab

The basic machined product in a form of a plate with various thicknesses, miscellaneous surface finishes, in minimal dimensions 250 x 120 cm.

### Format

The machined product prepared by cutting the material from original size into the form of format, with various thicknesses, dimensions and surface finishes.

### Final product

The product in the form of a slab or a format after the machining on the final production-line.

### Surface finish

The machining of the product surface on the final production-line primarily through sand-blasting, honing, brushing/antique finishing or polishing. Defined by the VP 04-10 Technical standard for engineered stone.

### Aesthetic parameters

Visual, assessable appearance of the product surface including the color shade, color structure and structural elements.

### Inert materials

(Also granulates) A set of inorganic, hard, polishable raw materials with natural features (siliceous sands, granites, quartzes...) or with industrial features (mirror iron, glass...) in the form of sorted grains of various fractions, constituting the main part of the product.

# General product information

## Product composition

The engineered stone Technistone is produced from inert materials (granulates – crushed granites, crushed quartz, crushed mirrors, siliceous sand, etc.), fillers (micronized siliceous raw material), binders (polyester resin), from color pigments and other additives.

## Description of the production technology

The production technology of the engineered stone Technistone is based on two production operations – the production of the semi-finished product (pressing line) and its machining to the final product (finalizing line).

### Production of the semi-finished product

Weighed quantities of certain prepared inert materials, filler, binder and pigments are intermixed. A slab of a defined thickness is prepared from the resulting mixture by the vibrational compression. The binder is hardened in the mixture by a thermal treatment.

### Machining of the semi-finished product

The surface of the semi-finished product is prepared according to the required level of machining by sand-blasting, calibrating, honing, polishing. The cutting of the product to the formats of defined dimensions and possible preparation of the edges is performed according to the requirements and needs.

### Product surface finish

The product surface can be finished step by step by the sand-blasting, honing, brushing/antique finishing upto semi gloss or mostly to high gloss.

(Sand) blasted finish: Treatment of the previously prepared faces of the product surface by blasting with the steel grit.

Honed finish: Machining of the previously prepared faces with an abrasive material.

Brushed and antique finish: Machining of the faces (prepared by pure brushing in advance by sand-blasting) with brushes.

Rough Brushed finish as option for swimming pools floor tiles: a variant of brushed finish with  rougher surface and consequently with higher antislipperness)

Semi-gloss: Machining of previously prepared faces with using abrasive material.

Polishing: Mechanical polishing of ground faces with abrasive material and polishing tools.

### Surface specification of the products with the surface finish: semi-gloss, honed, brushed, antique finish and sand-blasted finish

The product surface by semi-gloss or honed variant is matt, with marks remaining after the application of the last previous stage caused with honing (polishing) segments. These marks – continuous „soft scratches“ organized in wide bands building an antislipperness surface finish - are allocated on the product surface in regular interconnected cycles. The product surface may be covered by a thin layer of a dry, brushed-away material originating from the honing mechanism.

The product surface by sand-blasted variant is matte, grooved by the sand-blasted process, it may be covered by a thin layer of a dry, brushed-away material originating from the blasting mechanism.

The product surface by brushed and antique finish variant is grooved, it may also contain protruding or depressed grains exposed during the technological process. The surface may be covered by a thin layer of a dry, brushed-away material originating from the mechanism.

## Production groups of the engineered stone Technistone

The engineered stone Technistone is categorized into four basic production groups according to the predominant inert material.

| Production group | Sand | Granite | Mirrors | Crystal |
| --- | --- | --- | --- | --- |
| Predominant inert materials | Siliceous sands | Granites + siliceous sands | Mirror chips + siliceous sands | Siliceous sands + quartzes |
| Commercial names | Gobi | Taurus, Vesta, Kalahari, Vesuv, Sonora, Karpat, Basalt | Starlight | Crystal |

# Technical parameters of the product

## Dimensions of the product

The production process results in a slab with dimensions 305 x 134 cm or 306 x 141 cm. Guaranteed usable surface is defined by other parts of General Commercial Terms.

From these rough dimensions a whole-format product can be prepared in the form of a slab – in the basic dimensions up to 300 x 132 cm or 303 x 140, or other elements may be cut to the so-called formats. The basic dimensions of the formats are 30 x 30 cm, 40 x 40 cm and 60 x 60 cm.

The products can be manufactured in thickness from 10 up to 30 mm, the standard thickness being 10, 20 and 30 mm. Other possible thickness is e.g. 11, 12, 13, 14 mm.

## Dimension tolerations of formats

Table 1: Maximal permitted dimension tolerations of formats

| Length, width | Thickness | Rectangularity | Face flatness | Side flatness |
| --- | --- | --- | --- | --- |
| ±1 mm | ±1 mm (not applicable for the brushed, antique finish and blasted surface finish) | 1 mm on 1 running meter (LM) of a side | 1,3 mm on 1 running meter (LM) of the diagonal | 0,5 % |

## Dimension tolerations of the slab

Thickness: + 1,0 mm / - 1,2 mm.

## Basic technical requirements on the physical and mechanical characteristics of the product

The physical and mechanical properties of the product must comply with the basic technical requirements stated in internal VP 04-10 Technical Standard for engineered stone. The tests are performed on the machined product not earlier than 24 hours after the production of the semi-finished product. (The requirements for the absorbability are set at the level of surface machining: polishing; the requirement for the flexural strength is set for the thickness 10 mm of the test sample.)

| Production group | Density (minimal) | Absorbability after 48 hours AoP48 (maximal) | Flexural strength (minimal) | Abrasive power max . | Thermal expansion coefficient ά ( +20 to +70 °C ) max. | Thermal contraction coefficient ά ( - 20 to + 20 °C ) max. |
| --- | --- | --- | --- | --- | --- | --- |
|  | ( g / cm3 ) | ( % by weight ) | ( MPa ) | ( mm ) | ( 10-6 / °C ) | ( 10-6 / °C ) |
| Sand | 2,30 | 0,06 | 40 | 3 | 40 | 22 |
| Granite | 2,30 | 0,09 | 30 | 5 | 35 | 18 |
| Mirrors | 2,20 | 0,07 | 25 | 5 | 40 | 18 |
| Crystal | 2,05 | 0,07 | 35 | 3 | 43 | 33 |
| Implementation standard | Technical specification based on ČSN 72 1154 | Technical specification based on ČSN 72 1155 | ČSN EN 14617-2 | ČSN 72 1158 | Technical specification based on ČSN EN ISO 10545-8 , | Technical specification AZL 03 |

## Average values of basic physical and mechanical characteristics of the production groups

| Production group | Absorbability 48 hours (average) | Absorbability 48 hours (average) | Flexural strength | Abrasive power ∆ l (values - range) | Thermal expansion coefficient ά (+20 to +70 °C, range) |
| --- | --- | --- | --- | --- | --- |
|  | (% by weight) | (% by weight) | (MPa) | (mm) | (10-6 / °C) |
| Sand | 0,024 | 0,023 | 62 | 1,3 | 25,1 – 27,5 |
| Granite | 0,035 | 0,033 | 42 | 1,1 – 2,1 | 21,0 – 29,7 |
| Mirrors | 0,025 | 0,023 | 45 | 2,0 – 3,4 | 20,1 – 29,0 |
| Crystal | 0,023 | 0,020 | 51 | 2,1 | 27,8 – 35,3 |
| Implementation standard | ČSN 72 115 | ASTM C 97 | ČSN EN 14617-2 | DIN 52108 | ČSN EN ISO 10545-8 |
| Related standards | DIN 52 103 UNI 10444 | - | ASTM C 120 ASTM C 880 DIN 52 112 UNI 10443 | - | - |
| Stated | Technistone a.s., laboratory 2004 - 2005 | Stone and gravel test plant Hořice, 2002 - 2003 |

## Other values of the physical and mechanical, chemical, hygienic and fire characteristics of the product

The following tests were performed in certified test laboratories or in the laboratory of the Technistone company. Each summary table is provided with the source and year of measurement.

The results represent the properties of the engineered stone Technistone.

In case of need it is possible on request to up-to-date results and pass them on the distributor or the cutomer.

### Average mass of Technistone products

(The calculation was performed by taking the average density of all products: 2405 kg/m3. The mass of a respective product can be determined from the values given in the section: 4.6.2.)

| Length (cm) | Width (cm) | Thickness (mm) | Mass (kg) | Thickness (mm) | Mass (kg) | Thickness (mm) | Mass (kg) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 10 | 10 | 10 | 0,2 | 20 | 0,5 | 30 | 0,7 |
| 15 | 15 |  | 0,5 |  | 1,1 |  | 1,6 |
| 20 | 20 |  | 1,0 |  | 1,9 |  | 2,9 |
| 30 | 30 |  | 2,2 |  | 4,3 |  | 6,5 |
| 40 | 40 |  | 3,8 |  | 7,7 |  | 11,5 |
| 50 | 50 |  | 6,0 |  | 12,0 |  | 18,0 |
| 60 | 30 |  | 4,3 |  | 8,7 |  | 13,0 |
| 60 | 40 |  | 5,8 |  | 11,5 |  | 17,3 |
| 60 | 60 |  | 8,7 |  | 17,3 |  | 26 |
| 100 | 100 |  | 24 |  | 48 |  | 72 |
| 304 | 134 |  | 98 |  | 196 |  | 294 |

### Average density values

| Product name | Production group | Density (kg/m3) | Product name | Production group | Density (kg/m3) |
| --- | --- | --- | --- | --- | --- |
| Gobi Grey | Sand | 2430 | Starlight Emerald | Mirrors | 2370 |
| Gobi White | Sand | 2430 | Starlight Green | Mirrors | 2380 |
| Gobi Black | Sand | 2420 | Starlight Grey | Mirrors | 2380 |
| Kalahari | Granite | 2430 | Starlight Red | Mirrors | 2390 |
| Karpat Arizona | Granite | 2330 | Starlight Ruby | Mirrors | 2270 |
| Karpat Platinum | Granite | 2440 | Starlight Sapphire | Mirrors | 2370 |
| Sonora Light | Granite | 2420 | Starlight Violet | Mirrors | 2370 |
| Taurus | Granite | 2480 | Starlight White | Mirrors | 2310 |
| Taurus Blue Bahia | Granite | 2430 | Starlight Yellow | Mirrors | 2280 |
| Taurus Brown Pearl | Granite | 2490 | Crystal Beach | Crystal | 2320 |
| Taurus Gold | Granite | 2440 | Crystal Creme Beige | Crystal | 2380 |
| Taurus Nordic | Granite | 2480 | Crystal Diamond | Crystal | 2310 |
| Vesta Negro | Granite | 2440 | Crystal Ivory | Crystal | 2450 |
| Starlight Aquamarine | Mirrors | 2380 | Crystal Quartz White | Crystal | 2380 |
| Starlight Azurite | Mirrors | 2380 | Crystal Porto | Crystal | 2420 |
| Starlight Black | Mirrors | 2350 | Crystal Rio | Crystal | 2420 |
| Starlight Blue | Mirrors | 2380 | Crystal Royal | Crystal | 2330 |
| Starlight Citrine | Mirrors | 2390 | Crystal Topaz | Crystal | 2440 |

Source: Technistone, Inc. laboratory, period 2004 – 2005, Implementation standard: ČSN 72 1154

### Strength characteristics

Average values of the flexural strength and of the breaking load for individual products

Applied standards: ČSN EN 14617-2

| Product names | Production groups | Average flexural strength (MPa) | Breaking load (N) |
| --- | --- | --- | --- |
|  |  |  | Specimen thickness 10 mm | Specimen thickness 20 mm | Specimen thickness 30 mm |
| Karpat Arizona, Taurus Brown Pearl | Granite | 37 | 2693 | 5004 | - |
| Taurus, Taurus Blue Bahia, Taurus Gold, Taurus Nordic, Vesta Negro, Starlight: Aquamarine, Azurite, Black, Blue, Citrine, Green Grey, Red, Violet | Granite, Mirrors, | 42 | 2922 | 5573 | 8109 |
| Kalahari, Sonora Light, Starlight: Emerald, Ruby, Sapphire, White, Yellow, Crystal Ivory, Crystal Quartz White, Crystal Topaz | Granite, Mirrors, Crystal | 47 | 3148 | 6443 | 10520 |
| Gobi Black, Crystal: Beach, Creme Beige, Diamond, Porto, Rio, Royal | Crystal, Sand | 52 | 3638 | 7459 | 10605 |
| Gobi Grey, Gobi White | Sand | 62 | 4380 | 8885 | 12598 |

Source: Technistone, Inc. laboratory, period 2004 – 2005

Average values of the flexural strength and of the breaking load for individual product groups

Applied standards: ČSN EN 14617-2

| Production group | Average flexural strength (MPa) | Breaking load (N) |
| --- | --- | --- |
|  |  | Specimen thickness 10 mm | Specimen thickness 20 mm | Specimen thickness 30 mm |
| Sand | 62 | 4380 | 8885 | 12598 |
| Granite | 42 | 2946 | 5431 | 8121 |
| Mirrors | 45 | 3049 | 6034 | 10412 |
| Crystal | 51 | 3433 | 7164 | 9895 |

Source: Technistone, Inc. laboratory, period 2004 – 2005

Note:

Breaking load F = load in the time of the specimen failure measured in N, read on the scale of the testing apparatus

Average values of the Impact resistance for individual products (drop test / impact test, steel ball with the mass of 1 kg)

Applied standard: UNI 9721/10 (10442)

| Product names | Production groups | Average flexural strength (MPa) | Height at failure (cm) | Work (J) | Height at failure (cm) | Work (J) | Height at failure (cm) | Work (J) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Specimen thickness 10 mm | Specimen thickness 20 mm | Specimen thickness 30 mm |
| Karpat Arizona, Taurus Brown Pearl | Granite | 37 | 27 | 2,6 | 52 | 5,0 | - |  |
| Taurus, Taurus Blue Bahia, Taurus Gold, Taurus Nordic, Vesta Negro, Starlight: Aquamarine, Azurite, Black, Blue, Citrine, Green Grey, Red, Violet | Granite, Mirrors, | 42 | 26 | 2,5 | 47 | 4,5 | 96 | 9,2 |
| Kalahari, Sonora Light, Starlight: Emerald, Ruby, Sapphire, White, Yellow, Crystal Ivory, Crystal Quartz White, Crystal Topaz | Granite, Mirrors, Crystal | 47 | 23 | 2,2 | 48 | 4,6 | 113 | 10,8 |
| Gobi Black, Crystal: Beach, Creme Beige, Diamond, Porto, Rio, Royal | Crystal, Sand | 52 | 23 | 2,2 | 49 | 4,7 | 135 | 12,9 |
| Gobi Grey, Gobi White | Sand | 62 | 24 | 2,3 | 75 | 7,2 | 205 | 19,6 |

Source: Technistone, Inc. laboratory, period 2004 – 2005

Average values of the Impact resistance for production groups (drop test / impact test, steel ball with the mass of 1 kg)

Applied standard: UNI 9721/10 (10442)

| Production groups | Height at failure (cm) | Work (J) | Height at failure (cm) | Work (J) | Height at failure (cm) | Work (J) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Specimen thickness 10 mm | Specimen thickness 20 mm | Specimen thickness 30 mm |
| Sand | 24 | 2,39 | 75 | 7,2 | 205 | 19,6 |
| Granite | 27 | 2,6 | 51 | 4,9 | 106 | 10,1 |
| Mirrors | 24 | 2,3 | 46 | 4,4 | 101 | 9,6 |
| Crystal | 22 | 2,1 | 48 | 4,6 | 135 | 12,9 |

Source: Technistone, Inc. laboratory, period 2004 – 2005

Prismatic compressive strength, modulus of compression, Poisson coefficient

| Production group / implementing standard | Prismatic compressive strength (MPa), range | modulus of compression (MPa), range | Poisson coefficient, range |
| --- | --- | --- | --- |
|  | ČSN 72 1163 | ČSN 72 1165 | ČSN 72 1165 |
| Sand | 184 - 188 | 39,3 | 0,21 |
| Granite | 147 - 177 | 31,3 – 38,2 | 0,25 |
| Mirrors | 155 - 172 | 33,2 – 39,3 | 0,25 – 0,30 |
| Crystal | 188 - 195 | 31,7 – 34,9 | 0,18 – 0,20 |

Source: TZÚS Praha – subsidiary Brno, period 2003

Ultimate tensile strength, modulus of elasticity in tension

| Product | Production group / implementation standard | Ultimate tensile strength (MPa), average value | Modulus of elasticity in tension (MPa), average value |
| --- | --- | --- | --- |
|  |  | ČSN EN ISO 527 – 1, 2 |
| Gobi white | Sand | 36 | 40,0 |
| Taurus | Granite | 21 | 40,8 |
| Starlight Black | Mirrors | 19 | 32,6 |
| Crystal Quartz White | Crystal | 28 | 39,1 |

Source: Synpo, Inc. Pardubice, period 2004

Compressive strength, flexural strength, breaking load (breaking force) according to ASTM

| Production group / implementation standard | Compressive strength (PSI) | Flexural strenght in tension (PSI), | Breaking load (lbs) |
| --- | --- | --- | --- |
|  | ASTM C 170 | ASTM C 880 | ASTM C 648 |
|  | dry | wet | dry | Wet |  |
| Sand | 29,89 | 29,89 | 7,82 | 8,31 | 1340 |
| Granite | 24,50 | 21,35 | 5,04 | 5,20 | 1309 |
| Mirrors | 22,08 | 15,76 | 4,74 | 4,87 | 1207 |

Source: Smith-Emery Laboratories, Washington, period 1999 – 2000

Loading tests in accordance with ČSN 73 2046, ČSN 73 2030

| Product name | Production group | Achieved loading capacity Múexp (kN) | Manner of failure |
| --- | --- | --- | --- |
| Taurus | Granite | 7,7 | fracture |
| Crystal Quartz White | Crystal | >10,4 | without failure |

Source: TZÚS Praha – subsidiary Brno, period 2003

Test description: A product specimen with dimensions 60 x 60 x 2 cm was placed onto corner supports. A loading force (measured in kN) was applied to a steel plate with dimensions 10 x 10 cm, which was laid on the centre of the product.

### Thermal expansion coefficient of the product

Thermal expansion coefficient according to ASTM C 531-00, temperature range +20 / +100°

| Product name | Production group | Thermal expansion coefficient ά(10-6 °C-1) |
| --- | --- | --- |
| Gobi Grey | Sand | 27,5 |
| Kalahari | Granite | 25,6 |
| Karpat Arizona | Granite | 29,7 |
| Taurus | Granite | 22,0 |
| Starlight Blue | Mirrors | 20,1 |
| Starlight Sapphire | Mirrors | 22,8 |
| Starlight White | Mirrors | 27,4 |
| Crystal Quartz White | Crystal | 31,9 |

Source: Centro Ceramico Bologna., period 2002 – 2003

Thermal expansion coefficient according to ČSN 64 0528, temperature range +20 / +70°

| Product name | Production group | Thermal expansion coefficient ά(10-6 °K-1) |
| --- | --- | --- |
| Gobi Grey | Sand | 28,5 |
| Taurus Brown Pearl | Granite | 21,0 |
| Taurus Kongo | Granite | 22,7 |
| Starlight Black | Mirrors | 23,3 |
| Starlight Sapphire | Mirrors | 23,2 |
| Starlight White | Mirrors | 27,0 |
| Crystal Diamond | Crystal | 25,3 |
| Crystal Topaz | Crystal | 27,7 |

Source: TZÚS Praha – subsidiary Předměřice, period 2002 – 2005

Thermal expansion coefficient according to the Mapei specification,

temperature range +20 / +63°C

| Product name | Production group | Max. measured length difference (%) | Calculated thermal expansion coefficient ά(10-6 °C-1) |
| --- | --- | --- | --- |
| Gobi Grey | Sand | 0,105 | 28 |
| Karpat Arizona | Granite | 0,130 | 35 |
| Sonora Light | Granite | 0,080 | 22 |
| Taurus Blue Bahia | Granite | 0,110 | 30 |
| Vesta Negro | Granite | 0,080 | 22 |
| Starlight Blue | Mirrors | 0,060 | 16 |
| Starlight Sapphire | Mirrors | 0,071 | 19 |
| Starlight White | Mirrors | 0,075 | 20 |
| Crystal Quartz White | Crystal | 0,130 | 35 |

Source: Mapei Milano, period 2002

Note: the usage of the thermal expansion coefficient ά during the calculation

relation:  ∆1 = ∆ x (c2 – c1) x l0

∆1 = length difference (mm)

ά = thermal expansion coefficient

c2 = final temperature (°C)

c1 = initial temperature (°C)

l0 = initial length (mm)

Example: tile Taurus Brown Pearl 40 x 40 cm, temperature change from 20 to 70 °C. The length difference ∆1 0,42 mm of the tile is calculated after substitution of the relevant values into the relation. According to that a tile will be 400,42 mm long at the temperature of 70 °C (ά = 21x10-6, c2 = 70 °C, c1 = 20 °C, l0 = 400,0 mm).

### Dimensional stability of the product

Dimensional stability of the product under wet conditions according to the specification of the Mapei company

| Production group | Maximum deviation (mm) | Class |
| --- | --- | --- |
| Sand | 0,01 – 0,05 | A |
| Granite | 0,05 – 0,09 | A |
| Mirrors | 0,06 – 0,09 | A |
| Crystal | 0,03 – 0,09 | A |

Source: Mapei Milano, period 2002

Voluminal stability of the product – flatness, under wet conditions

Time of storage under wet conditions: 1 month, product with dimensions of 30 x 30 x 2 cm laid horizontally with its back face on a continuously wet mop

| Production group | Average change of flatness (mm) |
| --- | --- |
| Granite | 0,25 |
| Mirrors | 0,12 |
| Crystal | 0,25 |

Source: TZÚS Praha – subsidiary Brno, period 2004, implementation standard: ČSN EN 1339

Voluminal stability of the product – flatness, under wet conditions

Time of storage under wet conditions: 3 months, product with dimensions of 40 x 40 cm inserted vertically into water column of 20 cm

| Production group | Average of maximal measured flatness deviations (mm) |
| --- | --- |
|  | Specimen thickness 10 mm | Specimen thickness 20 mm |
| Sand | 0,2 | 0,1 |
| Granite | 0,2 | 0,2 |
| Mirrors | 0,2 | 0,2 |
| Crystal | 0,2 | 0,2 |

Source: Technistone, Inc. laboratory, period 2004, applied standard: ČSN EN 1339

### Physical tests of surface resistance

Mohs's hardness

| Production group / implementation standard | EN 101 | ČSN EN 101 | DIN EN 101 |
| --- | --- | --- | --- |
| Sand | 6 - 7 | 7 | - |
| Granite | 6 - 7 | 7 | - |
| Mirrors | 6 - 7 | 6 | 7,0 |
| Crystal | 6 - 7 | 7 | - |

Source: Stone and gravel test plant Hořice, Baustoffprufstelle Wismar GmbH, period 1999 – 2002

Abrasive power of the surface, wear resistance

| Test | Abrasive power ∆l (mm) | wear resistance (mm3) | wear resistance of the surface (class OPO) | Abrasive power index | Loss of thickness (mm) | Abrasive power (cm3/50cm3) |
| --- | --- | --- | --- | --- | --- | --- |
| Production group / implementation norm | DIN 52 108 | DIN EN ISO 10545-6 | ČSN EN ISO 10545-7 | ASTM C 501 | DIN 18500 | DIN 18500 |
| Sand | 1,3 | - | 2 | 212 | 1 | 5,4 |
| Granite | 1,1 – 2,1 | - | 3 | 119 | 1 | 5,7 |
| Mirrors | 2,0 – 3,4 | 197,0 | 2 - 3 | 113 | 2 | 10,7 |
| Crystal | 2,1 | - | 3 | - | - | - |

Source: Stone and gravel test plant Hořice, Baustoffprufstelle Wismar GmbH, TZÚS Praha – subsidiary Plzeň, Smith-Emery Laboratories, Washington, period 1999 – 2002

### Thermal resistance of the surface

Resistance of the surface to thermal shocks, insulating capability of the product   (ČSN EN ISO 10545-9, cycle 10 x 145°C)

| Test | Resistance of the surface to thermal shocks | Insulating capability of the product [(m2K)/W] |
| --- | --- | --- |
| Product name | Production group | Implementing standard |
|  |  | ČSN EN ISO 10545-9 | DIN EN 104 | DIN 52612-1 |
| Gobi Grey | Sand | no damage | - | - |
| Taurus Gold | Granite | no damage | - | - |
| Starlight Sapphire | Mirrors | no damage | - | - |
| Starlight Blue | Mirrors | no damage | - | - |
| Starlight | Mirrors | - | no damage | 0,011 |
| Crystal White | Crystal | no damage | - | - |

Source: TZÚS Praha – subsidiary Plzeň, Baustoffprufstelle Wismar GmbH, period 2000 – 2002

Heat-shock resistance of the surface of the product

Heated metallic body with a monitored temperature and mass which is laid for a defined period of time on the surface of the product with a given thickness on the edge or on the plane of the product.

Verbal assessment of the state of the product surface:   A – no change / B – recognizable grain edges / C – cracking,    Verbal assessment of the change of the shade:      0 – shade without change, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of the shade.

Source: Technistone, Inc. laboratory, period 2004

Verbal assessment of the state of the product surface:   A – no change / B – recognizable grain edges / C – cracking,   Verbal assessment of the change of the shade:     0 – shade without change, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of the shade.

Source: Technistone, Inc. laboratory, period 2004

Verbal assessment of the state of the product surface: A – no change / B – recognizable grain edges / C – cracking,   Verbal assessment of the change of the shade: 0 – shade without change, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of the shade.

Source: Technistone, Inc. laboratory, period 2004

Verbal assessment of the state of the product surface: A – no change / B – recognizable grain edges / C – cracking,   Verbal assessment of the change of the shade: 0 – shade without change, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of the shade.

Source: Technistone, Inc. laboratory, period 2004

Verbal assessment of the state of the product surface: A – no change / B – recognizable grain edges / C – cracking,   Verbal assessment of the change of the shade: 0 – shade without change, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of the shade.

Source: Technistone, Inc. laboratory, period 2004

Verbal assessment of the state of the product surface: A – no change / B – recognizable grain edges / C – cracking,   Verbal assessment of the change of the shade: 0 – shade without change, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of the shade.

Source: Technistone, Inc. laboratory, period 2004

### Determination of the heat-shock resistance according to EN 14617-6

| Product name | Production group | Visual assessment | Outcomes of the measurements (+ values: increase, - values: decrease) |
| --- | --- | --- | --- |
|  |  | Surface changes | Color change | Mass change ( % ) | Change of the gloss of the product surface ( % ) | % reflectivity | Change of the flexural strength ( % ) |
| Gobi White | Sand | A | 2 | -0,05 | 1 | 101 | 3 |
| Taurus Brown Pearl | Granite | A - B | 1 | -0,07 | 1 | 101 | 10 |
| Vesta Negro | Granite | A - B | 1 | -0,08 | 0 | 100 | -3 |
| Taurus Gold | Granite | A - B | 2 | -0,07 | -2 | 98 | -2 |
| Starlight Green | Mirrors | B | 2 | -0,05 | -2 | 98 | -3 |
| Starlight White | Mirrors | B | 2 | -0,06 | -3 | 97 | 8 |
| Crystal Royal | Crystal | A | 2 | -0,05 | 0 | 100 | 8 |
| Crystal Creme Beige | Crystal | A | 2 | -0,06 | 1 | 101 | -2 |

Verbal assessment of the state of the product surface:  A – no change / B - recognizable grain edges / C - crack intrusion / D – surface desintegration / E – specimen destruction.  Verbal assessment of the change of the color shade:  0 – shade unchanged, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of shade.

Source: Technistone, Inc. laboratory, period 2005

### Antislipperness properties of the product surface

Antislipperness properties of the product surface according to the standard ČSN 725191 / prEN 13552

| Production group | Machining of the product | Static coefficient of friction | Dynamic coefficient of friction | Pendulum method |
| --- | --- | --- | --- | --- |
|  |  | dry | wet | dry | wet | dry | wet |
| Sand | Polished | 0,64 | 0,40 | 0,41 | 0,34 | 57 | 15 |
|  | Honed | 0,67 | 0,65 | 0,50 | 0,44 | 61 | 36 |
| Granite | Polished | 0,74 | 0,56 | 0,44 | 0,38 | 54 | 16 |
|  | Semi-gloss | 0,86 | 0,45 | - | - | - | - |
|  | Honed | 0,73 | 0,73 | 0,48 | 0,47 | 64 | 45 |
|  | Brushed | 0,57 | 0,56 | 0,63 | 0,64 | 60 | 44 |
|  | „Rough brushed“ | 0,76 | 0,71 | 0,60 | 0,54 | 75 | 60 |
| Mirrors | Polished | 0,84 | 0,35 | 0,43 | 0,33 | 58 | 15 |
|  | Semi-gloss | 0,91 | 0,44 | - | - | - | - |
|  | Honed | 0,77 | 0,62 | 0,51 | 0,47 | 58 | 38 |
|  | Brushed | 0,64 | 0,61 | 0,63 | 0,55 | 53 | 37 |
|  | Blasted | 0,71 | 0,70 | 0,72 | 0,67 | 66 | 58 |
| Crystal | Polished | 0,90 | 0,32 | 0,41 | 0,32 | 52 | 16 |
|  | Honed | 0,77 | 0,74 | 0,52 | 0,49 | 61 | 40 |

Source: TZÚS Praha – subsidiary Plzeň, period 2002 – 2005

Antislipperness properties of the product surface according to the standard ISO 10545-17 – comparison after the application of antislipperness agent

| Production group | Surface finish | Static coefficient of friction | Static coefficient of friction after the application of antislipperness agent |
| --- | --- | --- | --- |
|  |  |  | Greep | Antislip K 37 |
|  |  | dry Fd | wet Fw | dry Fd | wet Fw | dry Fd | wet Fw |
| Granite | Polished | - | - | 0,9 | 0,7 | 0,9 | 0,8 |
| Granite | Semi-gloss | 0,9 | 0,5 | 0,7 | 0,6 | - | - |
| Mirrors | Polished | 0,8 | 0,4 | 0,9 | 0,7 | 0,9 | 0,6 |
| Mirrors | Honed | 0,8 | 0,5 | 0,8 | 0,7 | - | - |

Source: TZÚS Praha – subsidiary Plzeň, period 2002 – 2004

Coefficient of sliding friction according to the ČSN 74 4507 standard

| Production group | Surface finish | Coefficient of sliding friction |
| --- | --- | --- |
|  |  | dry | wet |
|  |  | s | d | s | d |
| Sand | Semi Polished | 0,62 | 0,79 | 0,42 | 0,48 |
| Granite | Polished | 0,46 | 0,56 | 0,44 | 0,49 |
| Mirrors | Polished | 0,70 | 1,25 | 0,35 | 0,32 |
| Mirrors | Semi Polished | 0,57 | 0,78 | 0,42 | 0,46 |
| Mirrors | Honed | 0,48 | 0,63 | 0,51 | 0,57 |
| Crystal | Polished | 0,61 | 0,80 | 0,43 | 0,44 |

Source: Materials and footwear test plant Zlín, period 1999 – 2002

Coefficient of sliding friction

| Production group / implementation standard | according to prEN 13552, method D, pendulum | according to SATRA TM144 |
| --- | --- | --- |
|  | Surface finish | dry | wet | wet |
| Mirrors | Semi-gloss | 68 | 37 | 0,23 |
| Mirrors | Brushed | 53 | 37 | - |

Source: Ceram, Stoke-on-Trent, Satra technology centry, TZÚS Prague – subsidiary Pilsen, period 2001 – 2004

Static coefficient of friction according to ASTM, slip-resistance determination according to DIN

| Production group / implementing standard | Static coefficient of friction ASTM C 1028 | Slip-resistance |
| --- | --- | --- |
|  | without surface cleaning | after surface cleaning with the Hillyards agent | DIN 51130 (shoe) (ČSN 725191) |
|  | Surface finish | dry | wet | dry | wet | angle (°) | classification |
| Sand | Polished | 0,78 | 0,61 | 0,97 | 0,62 | - | - |
| Sand | Honed | - | - | - | - | 12,0 | R10 |
| Granite | Polished | 0,77 | 0,56 | 0,91 | 0,56 | - | - |
| Granite | Semi-gloss | - | - | - | - | 9,0 | R9 |
| Granite | Honed | 0,82 | 0,73 | 0,84 | 0,75 | 10,2 | R10 |
| Granite | Brushed | - | - | - | - | 15,0 | R10 |
| Granite | Rough Brushed | - | - | - | - | 27,2 | R12 |
| Mirrors | Polished | 0,90 | 0,58 | 0,99 | 0,59 | 7,0 | R9 |
| Mirrors | Semi-gloss | - | - | - | - | 11,0 | R10 |
| Mirrors | Honed | - | - | - | - | 13,0 | R10 |
| Mirrors | Brushed | - | - | - | - | 16,8 | R10 |
| Mirrors | Blasted | - | - | - | - | 29,8 | R12 |
| Crystal | Polished | - | - | - | - | 9,0 | R10 |

Source: Smith-Emery Laboratories, Washington, TZÚS Praha – subsidiary Plzeň, period 1999 – 2005

### Chemical durability of polished and brushed product surface

Determination of the chemical durability according to ČSN EN ISO 10545-13  (exposure time 12 days, polished surface)

| Product name | Production group | Chemical agent, concentration / assessment (abbreviations according to the standard) |
| --- | --- | --- |
|  |  | Ammonium chloride NH4Cl (100g/l) | Sodium hypochlorite NaClO (20 mg/l) | Hydrochloric acid HCl (3%) | Hydrochloric acid HCl (18%) | Citric acid (100 g/l) | Lactic acid (5%) | Potash lye KOH (30g/l) | Potash lye KOH (100g/l) |
| Gobi Grey | Sand | UA | UA | ULA | UHA | ULA | UHA | ULA | UHC |
| Taurus Gold | Granite | UA | UA | ULA | UHA | ULA | UHA | ULA | UHC |
| Starlight Sapphire | Mirrors | UA | UA | ULA | UHA | ULA | UHA | ULA | UHC |
| Starlight blue | Mirrors | UA | UA | ULA | UHA | ULA | UHA | ULA | UHC |
| Crystal White | Crystal | UA | UA | ULA | UHA | ULA | UHA | ULA | UHC |
| Verbal assessment – abbreviations explanation | no change | no change | no change | no change | no change | no change | no change | changes on surface |

Source: TZÚS Prague – subsidiary Pilsen, period 2002

UA, ULA, UHA –no visible changes

UB, ULB, UHB – visible changes on the planes created by cutting

UC, ULC, UHC –visible changes also on the face side

Determination of the chemical durability according to ČSN EN 106  (exposure time 28 days, polished surface)

| Product name | Production group | Chemical agent, concentration / assessment |
| --- | --- | --- |
|  |  | Ammonium chloride NH4Cl (100g/l) | Sodium hypochlorite NaClO (20 mg/l) | Standard cleaning solution | Copper sulphate Cu(SO4)2 (20mg/l) | Sulphuric acid H2SO4 (70%) | Lactic acid (5%) | Potash lye KOH (200g/l) |
| Gobi Grey | Sand | V | V | V | V | V | V | N |
| Taurus Gold | Granite | V | V | V | V | N | V | N |
| Starlight Sapphire | Mirrors | V | V | V | V | N | V | N |
| Starlight blue | Mirrors | V | V | V | V | V | V | N |
| Crystal White | Crystal | V | V | V | V | V | V | N |

Verbal assessment:            V – no visible changes

N – visible changes

Source: TZÚS Prague – subsidiary Pilsen, period 2002

Determination of the chemical durability according to ČSN EN 122, DIN EN 122  (exposure time 24 hours, polished surface)

| Product name | Production group | Chemical agent, concentration / durability class |
| --- | --- | --- |
|  |  | KMnO4 (10g/l) | Methylene blue (10g/l) | NH4Cl (100g/l) | Standard cleaning solution | NaClO (20 mg/l) | Cu (SO4)2 (20mg/l) | HCl (3%) | Citric acid (100 g/l) | KOH (30g/l) |
| Gobi Grey | Sand | 2 | 3 | - | - | - | - | - | - | - |
| Taurus Gold | Granite | 2 | 2 | - | - | - | - | - | - | - |
| Starlight Sapphire | Mirrors | 1 | 1 | - | - | - | - | - | - | - |
| Starlight blue | Mirrors | 3 | 2 | - | - | - | - | - | - | - |
| Starlight | Mirrors | 2 | 2 | AA | AA | AA | AA | AA | AA | B |
| Crystal White | Crystal | 2 | 2 | - | - | - | - | - | - | - |

Verbal assessment: 1 – stains are removed by water, 2 – stains are removed by cleaning agent, 3 – stains are not removed

AA – no visible changes, B – visible changes of color

Source: TZÚS Prague – subsidiary Pilsen, Baustoffprufstelle Wismar GmbH,  period 2000 - 2002

Determination of the stain resistance according to ČSN EN ISO 10545-14  (exposure time 24 hours, polished surface)

| Product name | Production group | Chemical, food agent, concentration / assessment |
| --- | --- | --- |
|  |  | Chrome green | Iodine (13g/l) | Olive oil | Tea | Red wine | Coffee |
|  |  | cleaning method | durability class | cleaning method | durability class | cleaning method | durability class | cleaning method | durability class | cleaning method | durability class | cleaning method | durability class |
| Gobi Grey | Sand | A | 5 | A | 5 | A | 5 | A | 5 | A | 5 | A | 5 |
| Taurus Gold | Granite | A | 5 | A | 5 | A | 5 | A | 5 | A | 5 | A | 5 |
| Starlight Sapphire | Mirrors | A | 5 | A | 5 | A, B | 4 | A | 5 | A | 5 | A, B | 4 |
| Starlight Blue | Mirrors | A | 5 | A | 5 | A | 5 | A | 5 | A | 5 | A, B, C | 3 |
| Crystal White | Crystal | A | 5 | A | 5 | A | 5 | A, B | 4 | A | 5 | A | 5 |

Verbal assessment:           durability classes:  5 (the best – stain is removed by water-wash = A)  /  4 (stain is removed by wash with cleaning agent with weak effects = B)  /  3 (stain is removed by wash with cleaning agent with strong effects = C)  /  2 (stain is removed by wash with 3% HCl = D)  /  1 (the worst – stain cannot be removed)

Source: TZÚS Prague – subsidiary Pilsen, period 2002

Cleaning methods: A = specimens are cleaned under running water for 5 minutes, B = specimens are cleaned manually by using a cleaning agent with weak effects, C = specimens are cleaned manually by using a cleaning agent with strong effects, D = the tested specimen is exposed to a suitable solution for 24 hours, then it is cleaned with running water

Durability of a polished product surface to chemicals with exposure time of 24 hours,  basis for test execution: ASTM C 650 standard

Verbal assessment: 0 – surface intact, 1 – weak change in the surface smoothness, 2 – initial surface erosion, 3 – strong erosion of the surface, 4 – specimen destruction

Source: Technistone, Inc. laboratory, period 1999 - 2000

Durability of a polished product surface to chemicals with exposure time of 24 hours,  basis for test execution: ASTM C 650 standard

Verbal assessment: 0 – surface intact, 1 – weak change in the surface smoothness, 2 – initial surface erosion, 3 – strong erosion of the surface, 4 – specimen destruction

Source: Technistone, Inc. laboratory, period 1999 - 2000

Durability of the color shade of a polished product surface exposed to chemicals (24 hours), basis for test execution: ASTM C

650 Verbal assessment: 0 – shade unchanged, 1 – weak change of shade, 2 – medium change of shade, 3 – strong change of shade

Source: Technistone, Inc. laboratory, period 1999 - 2000

Durability of the color shade of a polished product surface exposed to chemicals (24 hours), basis for test execution: ASTM C 650 standard

Verbal assessment: 0 – shade unchanged, 1 – weak change of shade, 2 – medium change of shade, 3 – strong change of shade

Source: Technistone, Inc. laboratory, period 1999 - 2000

Determination of stain resistance of the color shade of a polished product surface exposed to strong chemicals

(HF hydrofluoric acid – reacts with silicates)

| Product / Production group | Gobi White Sand | Crystal Quartz White Crystal | Starlight Red Mirrors | Starlight Sapphire Mirrors | Taurus Gold Granite |
| --- | --- | --- | --- | --- | --- |
| Exposure time (min / hours) |  |  |  |  |  |
| Chemical | HCl (10%) | HF (10%) | NaOH (10%) | HCl (10%) | HF (10%) | NaOH (10%) | HCl (10%) | HF (10%) | NaOH (10%) | HCl (10%) | HF (10%) | NaOH (10%) | HCl (10%) | HF (10%) | NaOH (10%) |
| 10 min | 0 | 3 | 1 | 0 | 3 | 0 | 0 | 3 | 0 | 0 | 4 | 0 | 0 | 4 | 0 |
| 30 | 0 | 4 | 1 | 0 | 3 | 0 | 0 | 3 | 0 | 0 | 4 | 0 | 0 | 4 | 0 |
| 60 | 0 | 4 | 1 | 0 | 3 | 0 | 0 | 3 | 0 | 0 | 4 | 1 | 0 | 4 | 0 |
| 2 hours | 0 | 4 | 1 | 0 | 3 | 1 | 0 | 3 | 1 | 0 | 4 | 2 | 0 | 4 | 1 |
| 5 | 0 | 4 | 2 | 0 | 3 | 2 | 0 | 3 | 1 | 0 | 4 | 3 | 0 | 4 | 2 |
| 10 | 0 | 4 | 3 | 0 | 3 | 2 | 0 | 3 | 2 | 0 | 4 | 3 | 0 | 4 | 3 |

Verbal assessment: 0 – shade unchanged, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of the shade

Source: Technistone, Inc. laboratory, period 2004

Determination of the resistance of the product’s polished surface finish to the loss of surface smoothness caused by exposure to strong chemicals

(HF hydrofluoric acid – reacts with silicates)

| Product / Production group | Gobi White Sand | Crystal Quartz White Crystal | Starlight Red Mirrors | Starlight Sapphire Mirrors | Taurus Gold Granite |
| --- | --- | --- | --- | --- | --- |
| Exposure time (min / hours) |  |  |  |  |  |
| Chemical | HCl (10%) | HF (10%) | NaOH (10%) | HCl (10%) | HF (10%) | NaOH (10%) | HCl (10%) | HF (10%) | NaOH (10%) | HCl (10%) | HF (10%) | NaOH (10%) | HCl (10%) | HF (10%) | NaOH (10%) |
| 10 min | 0 | 2 | 0 | 0 | 3 | 0 | 0 | 3 | 0 | 0 | 3 | 0 | 0 | 2 | 0 |
| 30 | 0 | 2 | 0 | 0 | 3 | 0 | 0 | 3 | 0 | 0 | 3 | 0 | 0 | 4 | 0 |
| 60 | 0 | 2 | 0 | 0 | 3 | 0 | 0 | 4 | 0 | 0 | 3 | 0 | 0 | 4 | 0 |
| 2 hours | 0 | 2 | 0 | 0 | 3 | 0 | 0 | 4 | 0 | 0 | 3 | 0 | 0 | 4 | 0 |
| 5 | 0 | 2 | 0 - 1 | 0 | 3 | 1 | 0 | 4 | 0 | 0 | 4 | 0 | 0 | 4 | 1 |
| 10 | 0 | 2 | 0 - 1 | 0 | 3 | 1 | 0 | 4 | 1 | 0 | 4 | 0 | 0 | 4 | 1 |

Verbal assessment: 0 – surface intact, 1 – weak change in surface smoothness, 2 – initial surface erosion, 3 – strong erosion of the surface, 4 – destruction of the specimen surface

Source: Technistone, Inc. laboratory, period 2004

Determination of stain resistance of the color shade of a polished product surface exposed to chromatic salts solutions, subsequent surface cleaning

(KMnO4 Potassium permanganate – dark purple 10% solution, K2Cr2O7 Potassium bichroman – orange and yellow 10% solution)

| Product / Production group | Gobi White Sand | Crystal Quartz White Crystal | Starlight Red Mirrors | Starlight Sapphire Mirrors | Taurus Gold Granite |
| --- | --- | --- | --- | --- | --- |
| Exposure time (min / hours) |  |  |  |  |  |
| Chemical | KMnO4 | K2Cr2O7 | KMnO4 | K2Cr2O7 | KMnO4 | K2Cr2O7 | KMnO4 | K2Cr2O7 | KMnO4 | K2Cr2O7 |
|  | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning |
| 10 min | 2 | C | 1 | A | 2 | C | 1 | A | 2 | C | 0 | A | 1 | C | 1 | A | 1 | C | 1 | A |
| 30 | 2 | C | 1 | A | 2 | C | 1 | A | 2 | C | 0 | A | 1 | C | 1 | A | 1 | C | 1 | A |
| 60 | 2 | C | 1 | A | 2 | C | 1 | A | 2 | C | 0 | A | 1 | C | 1 | A | 1 | C | 1 | A |
| 2 hours | 3 | C | 1 | A | 2 | C | 1 | A | 2 | C | 0 | A | 1 | C | 1 | A | 2 | C | 1 | A |
| 5 | 3 | C | 1 | A | 2 | C | 1 | A | 2 | C | 0 | A | 2 | C | 1 | A | 2 | C | 1 | A |
| 10 | 3 | C | 1 | A | 2 | C | 1 | A | 2 | C | 0 | A | 2 | C | 1 | A | 2 | C | 1 | A |

Verbal assessment of the shade change: 0 – shade unchanged, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of the shade.    Verbal assessment of the subsequent surface cleaning:   A stain is removed by water-wash /  B stain is removed by wash using a cleaning agent with weak effects (Jar)  /  C stain is removed by wash using a cleaning agent with strong effects (Bert 27 – Bellinzoni)  /  D stain cannot be removed

Source: Technistone, Inc. laboratory, period 2004

Determination of stain resistance of the color shade of a brushed product surface exposed to edibles and chromatic salts solutions, surface impregnated with the New Microkem DC 8 agent, subsequent surface cleaning

(KMnO4 Potassium permanganate – dark purple 10% solution, strong coffee and tea extracts, cooking oil)

| Product / Production group | Gobi Grey Sand | Taurus Nordic Granite |
| --- | --- | --- |
| Exposure time (min / hours) |  |  |
| Chemical | KMnO4 | tea | coffee | oil | KMnO4 | tea | coffee | oil |
|  | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning | shade | cleaning |
| 10 min | 2 | C | 0 | A | 0 | A | 0 - 1 | B | 0 | A | 0 | A | 0 | A | 0 - 1 | B |
| 30 | 2 | C | 0 | A | 0 | A | 0 - 1 | B | 0 | A | 0 | A | 0 | A | 0 - 1 | B |
| 60 | 2 | C | 0 | A | 0 | A | 0 - 1 | B | 0 | A | 0 | A | 0 | A | 0 - 1 | B |
| 2 hours | 2 | C | 0 - 1 | C | 0 - 1 | C | 0 - 1 | B | 0 - 1 | C | 0 | A | 0 | A | 0 - 1 | B |
| 5 | 2 | C | 0 - 1 | C | 0 - 1 | C | 0 - 1 | B | 1 | C | 0 | A | 0 | A | 0 - 1 | B |
| 10 | 3 | C | 0 - 1 | C | 0 - 1 | C | 0 - 1 | B | 1 | C | 0 | A | 0 | A | 0 - 1 | B |

Verbal assessment of the shade change: 0 – shade unchanged, 1 – slight change of shade, 2 – medium change of shade, 3 – strong change of shade, 4 – loss of the shade.   Verbal assessment of the subsequent surface cleaning:   A stain is removed by water-wash  /  B stain is removed by wash using a cleaning agent with weak effects (Jar)  /  C stain is removed by wash using a cleaning agent with strong effects (Bert 27 – Bellinzoni)  /  D stain cannot be removed

Source: Technistone, Inc. laboratory, period 2004

Determination of the chemical durability of the product according to EN 14617-10

| Production group | Product | Chemicals (concentration 0,5N) | Exposure time | % reflectivity | Durability class |
| --- | --- | --- | --- | --- | --- |
| Sand | Gobi white | HCl | 1 hour | 99,0 | C 4 |
|  |  |  | 8 hours | 98,1 |  |
|  |  | NaOH | 1 hour | 94,1 |  |
|  |  |  | 8 hours | 93,0 |  |
| Granite | Taurus brown pearl | HCl | 1 hour | 94,3 | C 4 |
|  |  |  | 8 hours | 89,9 |  |
|  |  | NaOH | 1 hour | 92,8 |  |
|  |  |  | 8 hours | 90,3 |  |
|  | Vesta negro | HCl | 1 hour | 99,1 | C 4 |
|  |  |  | 8 hours | 95,0 |  |
|  |  | NaOH | 1 hour | 98,8 |  |
|  |  |  | 8 hours | 89,5 |  |
|  | Taurus gold | HCl | 1 hour | 93,7 | C 4 |
|  |  |  | 8 hours | 88,6 |  |
|  |  | NaOH | 1 hour | 95,9 |  |
|  |  |  | 8 hours | 83,5 |  |
| Mirrors | Starlight green | HCl | 1 hour | 90,4 | C 4 |
|  |  |  | 8 hours | 88,5 |  |
|  |  | NaOH | 1 hour | 98,1 |  |
|  |  |  | 8 hours | 89,8 |  |
|  | Starlight white | HCl | 1 hour | 96,4 | C 4 |
|  |  |  | 8 hours | 91,7 |  |
|  |  | NaOH | 1 hour | 98,8 |  |
|  |  |  | 8 hours | 86,8 |  |
| Crystal | Crystal royal | HCl | 1 hour | 99,5 | C 4 |
|  |  |  | 8 hours | 95,5 |  |
|  |  | NaOH | 1 hour | 94,6 |  |
|  |  |  | 8 hours | 91,2 |  |
|  | Crystal creme beige | HCl | 1 hour | 93,7 | C 4 |
|  |  |  | 8 hours | 93,1 |  |
|  |  | NaOH | 1 hour | 93,1 |  |
|  |  |  | 8 hours | 85,1 |  |

The effect of exposure to chemicals is expressed by means of the decrease of reflectivity (gloss). The decrease is calculated as % of the reflectivity of the tested specimen in respect to a reference value (99 % of reflectivity means 1 % decrease in the gloss caused by the exposure to chemicals)

Durability class C 4 – change of % reflectivity from 100 to max. 80% - the highest possible durability class

Source: Technistone, Inc. laboratory, period 2005

### Resistance of the surface of the Technistone product to water and chemical defrosting agents exposure

Method A – automatic looping, 100 defrosting loops, defrosting agent – 3% NaCl

| Production group | Test result | Visual change of the color shade or gloss of the product surface |
| --- | --- | --- |
| Sand | Conforms | Not observed |
| Granite | Conforms | Not observed |
| Mirrors | Conforms | Not observed |
| Crystal | Conforms | Not observed |

Source: TZÚS Prague – subsidiary Předměřice, period 2004, implementation standard: ČSN 73 1326

### Technical fire characteristics of the product

Determination according to the ČSN standards

| Determination | Flammability | Index of flame spread is | Ignition temperature | Firing point | Combustion heat | Heating capacity |
| --- | --- | --- | --- | --- | --- | --- |
| Unit | - | mm/min | °C | °C | MJ/kg | MJ/kg |
| Implementation standard | ČSN 73 0862 | ČSN 73 0863 | ČSN 64 0149 | ČSN 64 0149 | ČSN ISO 1928 | ČSN ISO 1928 |
| Engineered stone Technistone | B – hardly flammable | 30,4 | 445 | 550 | 2,24 | 2,11 |

Source: Pavus, Inc., Technical fire laboratory Praha, period 2002 – 2003

Determination according to the standards ASTM and DIN

| Determination | Index of flame spread | Index of smoke development | Flammability | Heating capacity |
| --- | --- | --- | --- | --- |
| Unit | - | - | - | kJ/kg |
| Implementation standard | ASTM E 84-97a | ASTM E 84-97a | DIN 4102-1 | DIN 51900 |
| Production group Granite | 10 | 115 | - | - |
| Production group Mirrors | - | - | B 1 – flammable with difficulty | 2102 |

Source: Baustoffprufstelle Wismar GmbH, Smith-Emery Laboratories, Washington, period 1999 – 2002

### Hygienic properties of the product

National health institute of the  Czech Republic, Health and living conditions centre issued a Certificate of the health harmlessness of the Technistone product based on an expertise.

The product was certified by the NSF International organization with the following outcome: the product is in compliance with the 51 NSF/ANSI Standard – Food equipment materials, Solid surfaces for Splash zone.

### Frost resistance

Determination of the frost resistance according to EN 14617-5

| Product name | Production group | Measurement outcomes (+ values: increase, - values: decrease) |
| --- | --- | --- |
|  |  | Change of the flexural strength after frost load (%) |
| Gobi White | Sand | 13 |
| Taurus Brown Pearl | Granite | 5 |
| Vesta Negro | Granite | 1 |
| Taurus Gold | Granite | -2 |
| Starlight Green | Mirrors | 6 |
| Starlight White | Mirrors | 11 |
| Crystal Royal | Crystal | 17 |
| Crystal Creme Beige | Crystal | 11 |

Source: Technistone, Inc. laboratory, period 2005

# Recommended use of the product

The engineered stone Technistone may be used for small-sized or large-sized wall and floor  cladding, interior components, construction elements, furniture and supplementary components.

The product is recommended for interior use.

## Installation

To use the product for interior installation it is necessary to follow these recommendations:

### Recommended thickness depending on the dimension of the format (of the standardly loaded area)

| Product dimensions ( cm ) | Minimal recommended product thickness (mm ) |
| --- | --- |
| up to 60 x 60 | 10 |
| larger and non-standard dimensions | the solution has to take the project conditions, installation and load into account 12 – 20 mm |

### The influence of the surface finish on the antislipperness properties of the product (installation)

| Increase of slip-resistance | Surface finish |
| --- | --- |
| ( | Blasted |
|  | Rough brushed |
|  | Brushed, Antique/brushed |
|  | Honed |
|  | Semi-gloss |
|  | Polished |

### Suitability of the usage of the product at higher mechanical load

(including industrial, abrasive and travelling dynamic loading)

| Load increase / increase of the suitability of usage | Production group | Product thickness (mm) | Product color | Surface finish |
| --- | --- | --- | --- | --- |
| ( | Sand | 14 | Polychrome | Brushed, Antique/brushed |
|  | Crystal | 13 | Light monochromatic | Blasted |
|  | Granite | 12 | Dark monochromatic | Honed, Semi-gloss |
|  | Mirrors | 10 | White | Polished |

### Suitability of the usage of the product at high thermal load

(floor heating, permanent exposure to sunlight, alternation of high and low temperatures - entrances)

| Load increase / increase of the suitability of usage | Production group | Product thickness (mm) | Product color | Granularity of the product |
| --- | --- | --- | --- | --- |
| ( | Granite | 14 | White | Coarser |
|  | Mirrors | 13 | Light |  |
|  | Crystal | 12 | Darker | Medium |
|  | Sand | 10 | Dark | Fine |

### Recommended thickness of the format according to the dynamic (travelling) load of the face/true side

(resistance to damage, strain…)

| Average flexural strength (MPa) | Product | Thickness of the format (mm), classification into groups |
| --- | --- | --- |
|  |  | 6 mm | 9 mm | 10 mm | 11 mm | 12 mm | 13 mm | 14 mm | 20 mm |
| 37 | Karpat Arizona, Taurus Brown Pearl | 1 | 2 | 2 | 3 | 3 | 3 | 4 | 5 |
| 42 | Taurus, Taurus Blue Bahia, Taurus Gold, Taurus Nordic, Vesta Negro, Starlight: Aquamarine, Azurite, Black, Blue, Citrine, Green Grey, Red, Violet | 1 | 2 | 3 | 3 | 3 | 4 | 4 | 5 |
| 47 | Kalahari, Sonora Light, Starlight: Emerald, Ruby, Sapphire, White, Yellow, Crystal Ivory, Crystal Quartz White, Crystal Topaz | 1 | 2 | 3 | 3 | 4 | 4 | 4 | 5 |
| 52 | Gobi Black, Crystal: Beach, Creme Beige, Diamond, Porto, Rio, Royal | 1 | 3 | 3 | 3 | 4 | 4 | 4 | 5 |
| 62 | Gobi Grey, Gobi White | 2 | 3 | 3 | 4 | 4 | 4 | 5 | 5 |

Classification, specification and use of groups

Group 1: residences without travelling load

Group 2: public, commercial and industrial buildings with irregular transport by vehicles with inflatable tyres

Group 3: public, commercial and industrial buildings with transport by vehicles with elastic rubber tyres

Group 4: public, commercial and industrial buildings with transport by vehicles with hard plastic wheels

Group 5: public, commercial and industrial buildings with transport by vehicles with hard plastic wheels with very high load

Cleaning machines are meant under the term transport, too.

The recommended literature for this problem domain is the publication „Mechanisch hoch belastbare keramische Bodenbelage“ - ZDB Germany 2002 (Ceramic flooring with high mechanical load capacity).

### The recommended use of the individual production groups of the Technistone product and its dependence on the expected abrasive loading of the product

| Abrasive load of the floor | Recommended production group |
| --- | --- |
|  | Sand | Granite | Mirrors | Crystal |
| High | yes | yes | yes 1 | yes |
| Medium | yes | yes | yes | yes |
| Low | yes | yes | yes | yes |

1  the surface finish – polished - may not be used!

| Abrasive load of the floor | Recommended surface finish |
| --- | --- |
|  | Blasted | Brushed | Honed | Semi-gloss | Gloss |
| High | yes | yes | Yes | yes | no |
| Medium | yes | yes | Yes | yes | yes |
| Low | yes | yes | Yes | yes | yes |

At medium and high loading, installation of a cleaning zone and regular curing of the product in use is necessary.

Examples of the dependence of the use of the product on its abrasive load:

High load (heavy traffic + high presence of abrasive and liquid contaminants)

- installed in entrances and exits from the buildings and halls, in front of cash desks, receptions, counters, in underpasses, covered platforms, etc.

Medium load (heavy traffic without higher presence of abrasive contaminants)

- installed in shops, offices, halls, corridors, etc.

Low load (medium traffic without the presence of abrasive contaminants)

installed in residences, internal offices, halls, decorative places, etc.

## Raised floors

When placing the product on the grates of raised floors it is necessary to follow the following recommendation:

Recommended thicknesses:

| Recommended product dimensions (cm) | Minimum recommended product thicknesses (mm) |
| --- | --- |
| up to 60 x 60 | 20 |
| more than 60 x 60 | 30 |

## Wall cladding

All product types and all surface finishes are appropriate for inner wall cladding. It is necessary to take the mass of the product into account, see section:4.6.1 .)

Recommended thicknesses and dimensions

Glued installation

(recommended height up to max. 2,5 m)

| Recommended dimensions of the product (cm) | Recommended thickness of the product (mm) |
| --- | --- |
| 30 x 30 | 10 |

Cladding on supporting mounted grates

| Recommended dimensions of the product (cm) | Recommended thickness of the product (mm ) |
| --- | --- |
| according to the used system and product | 10 - 20 |

Anchored cladding

| Dimensions of the product (cm) | Minimum recommended thickness of the product (mm) |
| --- | --- |
| up to 60 x 60 | 30, exceptionally 20 (according to the system) |
| more than 60 x 60 | 30 |

## Stair components

When using the product for stair components it is necessary to follow this recommendation:

Recommended thicknesses :

| Way of laying down the component | Minimum recommended thickness of the product (mm) |
| --- | --- |
| whole face on substrate concrete | 10 - 20 |
| into construction, self-supporting | 30 |

All production groups of the engineered stone are suitable for usage as a stair component. Attention is to be paid to the antislipperness finish of the step-on surface. For each concrete application of the product its dimensions must always be considered in relation to its physico-mechanical characteristics and with respect to the system of fixing the product.

## Worktops

When using the product for worktops it is necessary to follow these recommendations:

the larger the thickness of the product, the higher its strength and thermal resistance

the hardness of the product surface and in virtue of it also the long-term resistance against mechanical damage of the surface is given by the raw materials used (see section: 5.5.1)

the product surface is not infinitely resistant to strokes of hard (especially metallic) objects, or to the drops of hard (especially metallic) objects

during selection of the product it is always necessary to take into account its characteristics (raw materials used) and the expected use and load of the final worktop (see section: 5.5.1)

hot objects are not to be laid directly onto the surface of the worktop (see section: 5.5.2)

the gloss and color shade of the product may be disturbed by the exposure to some chemicals

the fluorhydric acid causes an immediate erosion of the product surface layer

some strongly coloring substances can change the color shade of the product locally

the product reaches the highest resistance of the surface with the surface finish - polished

### Recommendation of the usage of individual production groups for the worktops

| Usage type | Example usage place | Sand | Crystal | Granite | Mirrors |
| --- | --- | --- | --- | --- | --- |
| Common usage | Kitchen countertops, tables, bar countertops…. | Yes | Yes | Yes | Yes |
| Higher and more frequent mechanical stress of the surface | Shops, sculleries, manufacturing plants, issue counters | Yes | Yes | Yes | No |
| Thermal load | Cooling, heating | Yes | Yes | Yes | No |
| Chemical load | Laboratories | Yes | Yes | No | No |

### Recommended usage of insulating pads against the thermal shock

(holds also for the use of the product as worktop of the kitchen furniture)

It is necessary to use insulating pads for putting off hot objects onto the surface of the product. These pads must also be placed below all cooking and baking appliances located on the kitchen counter.

The usage of insulating pads is necessary especially:

when the thickness of the counter is smaller than 30 mm

when one is putting off hot objects near the edges and cut-outs of the counter

when one is using cooking and baking appliances located on the kitchen counter

when one is using coarse-grained Technistone products

when one is using a product belonging to the production group Mirrors.

## Other usage

All the production groups of the engineered stone are suitable for usage as interior components. Dimensions of the used product must always be considered in relation to its physico-mechanical characteristics and with respect to the system of fixing the product. Regarding the resistance to aggressive influences (e.g. exposure to chemicals) the usage of products with characteristics reflecting the aggression of the surrounding environment is recommended. The degree of the surface finish of the product is to be chosen with respect to the expected usage of the product.

# Installation of the product

## General rules

During installation of the engineered stone Technistone it is necessary to conform to relevant standards, safety regulations of used products, recommendations of the producers of the bedding surface mixtures and of the producers of glues, jointing and dilatation materials (some of the recommendations are listed in the appendix of this document). Furthermore, it is necessary to assess and take into account the following facts, which are based on tests and practical experience. Only general hints are introduced here, because the manufacturer of the engineered stone has no influence on the individual building conditions and performance.

the product is intended for internal use

suitability of the individual product types of Technistone for the usage in the given environment especially with respect to the mechanico-physical characteristics of the Technistone products (e.g. a higher thermal expansion and contraction, lower absorbability...)

characteristics of the used product Technistone must be consistent with characteristics of all other used construction materials

the behaviour of the Technistone product after installation depends on the quality of the installation and fixation

during installation it is necessary to pay special attention to the quality of the bedding surface

carrying out jointless installation of the flooring and wall cladding from the Technistone product is strongly not recommended

it is recommended to have the Technistone product installed by a specialized company, which is experienced in installing the Technistone product, engineered or natural stone

it is necessary to adhere to the preparation technology and production procedures given by the producers of the used bedding mixtures, gluing and jointing materials and other used constructional chemicals

after jointing is performed it is necessary to stick to the technology of the product cleaning

## Installation of floor and wall tiles

### Recommended adhesives

The following adhesives are recommended by the producer for installation:

Elastorapid (Mapei)

Usage: at all standard installations of flooring and wall cladding.

Characteristics: Improved, quickly solidifying, two-part cementing binder (white and grey color), slip-resistant, with prolonged fading.

Classification according to EN 12004: class C2FTE

Classification according to EN 12002: class S2

Thickness of the layer of the adhesive: up to 10 mm.

Preparation: in accordance with the instructions of the producer.

Technical data (at +23°C and 50% relative humidity):

Acceptable temperature for application: from +5 to +30°C

Application life: 60 - 75 min.

Final setting time: 120 - 150 min.

Ascendability: after 4 hours.

Loadability: after 24 hours.

Increased loadability: after 48 hours.

Jointing: after 4 hours.

Spreading: toothed spatula (square-edged teeth).

Consumption: 3 - 6 kg/m2

Storage life: 12 / 24 months.

Granirapid (Mapei)

Usage: at all standard installations of flooring and wall cladding, especially when a quick solidification of the adhesive and a shorter waiting period for ascendability is needed.

Characteristics: Quickly solidifying, two-part cementing binder (white and grey color).

Classification according to EN 12004: class C2F

Thickness of the layer of the adhesive: up to 10 mm.

Preparation: in accordance with the instructions of the producer.

Technical data (at +23°C and 50% relative humidity):

Application life: 45 min.

Final setting time: 20 min.

Time, when corrections are possible: 45 min.

Ascendability: after 4 hours.

Loadability: after 24 hours.

Increased loadability: after 48 hours.

Jointing: after 3 hours.

Spreading: toothed spatula (square-edged teeth).

Consumption: 3 - 8 kg/m2

Storage life: 12 months.

Keralastic (Mapei)

Usage: in special cases – gluing on metal or wood, at stronger requirements for adherence, elasticity, waterproofness, at higher thermal loads, etc..

Characteristics: Two-part elastic waterproof polyurethane binder for gluing and jointing.

Preparation: in accordance with the instructions of the producer.

Technical data (at +23°C and 50% relative humidity):

Thermal resistance: - 40°C + 100°C

Application life:6 – 8 hours.

Final setting time: 2 hours.

Time, when corrections are possible: 3 hours.

Full loadability: after 7 days.

Jointing: after 12 hours.

Spreading: toothed spatula.

Consumption: 2 – 3,5 kg/m2

Storage life: 24 months.

Kerapoxy (Mapei)

Usage: when increased chemical durability is required, at higher thermal loads, at concurrent increased thermal and mechanical loads...

Characteristics: see section 6.2.2, jointing materials.

### Recommended jointing materials

At the installation the producer recommends to use the following jointing materials produced by the Mapei company:

Ultracolor

Cementing jointing material for joints 2 – 20 mm wide.

Kerapoxy

Two-part acidproof jointing material on the basis of epoxide resin. Use when the resistance to acids, chemical substances, solvents, wear and heavy operation is required and when water-impermeability and easy cleaning is required.

Mapesil AC

One-part silicone jointing and sealing material for permanently elastic joints in civil engineering. Available in many shades of color.

Mapeflex PU21

Two-part self-levelling sealing material for horizontal joints on the basis of polyurethane for permanently elastic sealing of dilatation and contact joints, for permanently elastic sealing of joints exposed to intense mechanical stress (supermarkets, car repair services, car showrooms...).

Mapeflex PU30

Thixotropic two-part sealing material for horizontal joints on the basis of polyurethane for permanently elastic sealing of dilatation and contact joints, for permanently elastic sealing of joints exposed to intense mechanical stress (supermarkets, car repair services, car showrooms...). Suitable for jointing oblique areas.

### Tools and instruments

To fulfil the installation the worker has to be equipped with at least these tools and instruments:

toothed spatula: to apply and spread uniformly the adhesive binders

smooth spatula: to rub the binder in the bedding and to spread a layer of the binder on the back face of a tile

angle, meter, ruler, water level, plumb, etc. for accurate measuring and levelling of the formats and slabs

lath batten, ruler, etc.: for fixing and continuously checking flatness of formats during installation

rubber or plastic spatulas: to apply and spread jointing material or binder

sponge: for correcting the smoothness and rubbing down the remains of jointing material from the tile

hammer, drilling machine, drills, sawing machine with diamond circular saw cooled down by water: for possible size adjustments or other correcions

boards, plywood, foil: to protect newly-installed floor tiles

## Beddings

### Generally

The preparation of beddings must be in compliance with the requirements of relevant standards and project documentation.

All beddings on which the product is installed must be dry, stable, solid, compression-resistant, sufficiently flat and cleared from removable particles, dry surface „cement laitance“, dust, fats, oils, wax, colors, dismantling chemical agents and everything that could decrease their adherence. These removable particles must be removed in the best case by sand blasting, (milling or honing also possible), which is followed by sucking up the remains with a vacuum cleaner. The beddings have to be suitable for the acceptance of the load and endure the stress expected in the specific application.

In the case of concrete floor beddings not only must structural joints be created, but also the dilatation joints or separation into ca 6 x 6 m large parts have to be accomplished, while taking into account the geometrical shape and seamless pouring of the concrete. The joints are obtained by mechanical cutting or by inserting plastic profiles and they must run through at least 1/3 of it. The circumferential joints must be taken into account in the proximity of all walls, columns, stairs etc. and their minimum width is 3 – 5 mm for all surfaces area of which is greater than 7 m2.

### Concrete

Sufficient maturing must be reached – at least 4 weeks! After the concreting is finished the concrete must be moistened properly and protected against too quick evaporation or against frost for at least 15 days. The humidity of the concrete must be at most 2 – 3% before the installation. The humidity is measured by a carbide moisture meter. Minimum compressive strength of the concrete amounts to 22 MPa, when higher loads of floors are expected it is necessary to achieve higher values of the strength. It is necessary to perform proper bottom damp-proofing. The surface must be strong, cohesive, without dust, see section 6.3.1. The strength in tension of the bedding (the strength of the surface layer) of the concrete is at least 0.8 MPa. The strength of the surface layer may be determined also by the Schmidt rebound hammer. It is necessary to apply bonding primer to the bedding (e.g. Primer of the Mapei company for starved beddings), other types of the penetration according to the absorption capacity of the bedding, which will increase the adherence of the used adhesive to the bedding.

### Usual cement finishes

The finish must be supporting and be at least 5 cm thick; the thickness depends on the expected load. It is composed of a concrete built up by inert heterogeneous material with the diameter from 0 to 8 mm and from general-use cement 425 kg/m3. Greater thickness requires inert material of greater diameter (up to ¼ of the thickness of the finish). After the finish is created it must be moistened properly and protected against too quick evaporation or against frost for at least 15 days. The minimum compression strength of the finish amounts to 22 MPa, when higher load of the floor is expected it is necessary to achieve higher values of the strength.

Sufficient maturing must be reached – at least 4 weeks! The humidity of the finish must be at most 2 – 3% before the installation. The humidity is measured by a carbide moisture meter. The surface must be strong, cohesive, without dust, see section 6.3.1. The strength in tension of the bedding (the strength of the surface layer) of the concrete is at least 0.8 MPa. The strength of the surface layer may be determined also by the Schmidt rebound hammer. It is necessary to apply bonding primer to the bedding (e.g. Primer of the Mapei company for starved beddings), other types of the penetration according to the absorption capacity of the bedding, which will increase the adherence of the used adhesive to the bedding.

### Cement finish Mapecem

Quick-setting and maturing cementing binder for creating floating and anchored finishes, on which the tiles have to be glued quickly. The thickness of the finish depends on the expected load. The installation of the engineered stone is possible after 24 hours.

### Cement finish Topcem

Special hydraulic binder for producing finishes. The installation of the engineered stone is possible after 7 days. The thickness of the finish depends on the expected load.

### Previously existing floors and facing

Cement floors or floors composed of old ceramics, floor tiles, marble, must be strong, well anchored to the bedding and without cracks. Cleaning from oils, waxes, fats, etc. must be performed in such a way, that their overall and also in-depth removal is guaranteed. Existing coatings must be removed.

### Metal

The bedding must be degreased by means of solvents of suitable cleaning agents. It is necessary to remove possible rust.

### Spattered dashes and plasters

They have to be sufficiently mature and strong to hold the weight of the tiles (when products are used, which are mixed in advance, it is necessary to follow the technical procedure described by the producer). The surface has to be dry, solid, without impurities and dust.

### Walls from blocks of expanded cement

Considering the great diversity of the products present on the market it is absolutely essential to consult producers, in order to learn about the properties and the suitability of their products. The surface must be dry, strong, without impurities and dust.

### Anhydride floors

They must be sufficiently mature and supporting. The strength of the surface layer may be determined also by the Schmidt rebound hammer.

The humidity of the anhydride floor must be at most 0,5% before the installation!! The humidity is measured by a carbide moisture meter. The surface must be strong, cohesive, without dust, see section 6.3.1.

The surface has to be penetrated two times by means of the Primer G agent (Mapei), in order to achieve a good adherence of the used adhesive to the bedding. After finishing the penetration it is necessary to wait until it dries.

## Levelling of bedding

In case of an uneven surface it is necessary to perform levelling or correction by using suitable levelling materials (e.g. Mapecem, Topcem, Ultraplan, Novoplan 21, Nivoplan, Nivorapid of Mapei company). Deviation from the flatness should be at most ±2 mm on 2 m of the surface. During the preparation and application of all levelling means the technical procedure described by the producer is to be followed strictly.

## Environment conditions at the installation

The installation can be started only after making sure that the temperature and moisture conditions meet the conditions prescribed by the technical brochures of the used adhesives.

For a longer period than 24 hours the temperature cannot decrease beneath +5 °C and exceed +30 °C.

The surfaces must not be strongly heated up by the sun before the installation (it is recommended to accomplish the installation during colder hours).

In a dry and ventilated environment it is necessary to pay special attention to a film creation on the adhesive.

It is necessary to spread the adhesive on small areas and check the moistening.

The bottom face of the formats must not be wet or dirty after previous cutting.

Every adverse situation is to be discussed with the work manager.

## Preparation of adhesives

It is necessary to use a clean vessel for the preparation of adhesives, binders, levelling finishes, etc.

To mix the agents it is necessary to use a mechanical agitator with small number of revolutions (approximately 150 rpm).

During mixing of all agents it is necessary to strictly follow the technical procedure described by the producer.

It is always necessary to add powder to a liquid and vice versa.

## Application of adhesives

First, the actual bedding is checked, for it has to be perfectly flat, dry, mature, without cracks, and carefully cleaned. Parts that are not tightly bound with the bedding have to be removed.

The preparation and application of the adhesive is performed according to the technical conditions of the producer.

The prepared adhesive must be perfectly homogeneous and easily spreadable. Always only such an amount is prepared, which is possible to apply before the adhesive starts to lose its adhesiveness and applicability.

The prepared adhesive is first well rubbed as a thin layer to the bedding by a smooth spatula to build a quality transition between the bedding, the adhesive and the tile. Only such an area will be prepared, which prevents drying of the surface layer of the adhesive at those places, where the tiles were still not installed. Afterwards the layer of the adhesive is spread on the bedding by a toothed spatula.

Recommended size of the toothed spatula:

| Size of the format | Size of the toothed spatula |
| --- | --- |
| 20 x 20 cm, 15 x 15 cm….. | 8 |
| from 40 x 40 cm (30 x 30 cm, 40 x 40 cm) | 10 |
| over 40 x 40 cm (60 x 30cm, 60 x 40 cm, 60 x 60 cm and larger) | 15 |

During the installation of the tile, the toothed spatula also delimits the thickness of the adhesive layer and by its individual teeth it creates a space for the uniform spread of the adhesive. The uniform spread of the adhesive during the installation of the tiles can be checked by a retroactive lifting off of the tile. The tooth-formed adhesive layer is continuously to be checked, whether it does not lose its adhesiveness (by a finger test).

It is necessary to use the system with double coating in such a manner that 100 % of the tile surface is glued-on. A continuous 1mm layer of the adhesive is applied on the bottom face of the tile and not until after that the gluing of the tile to the tooth-formed adhesive applied to the bedding will be accomplished.

During the installation of the slabbing the flatness is checked continuously.

The tiles should be installed with adherence to the joint from 3 up to 10 mm according to the characteristics of the bedding, the dimensions, dimensional stability and thermal expansion coefficient and according to the environment, where the installation takes place.

It is necessary to avoid vertical mismatch between individual tiles, especially at those places, where the dynamic loading of the area is expected (travelling of vehicles).

## Dilatation and dividing joints

During solution of the dilatation joints it is necessary to take into account the relevant standards, the project documentation and the characteristics of the product, especially its thermal expansion.

The dilatation joints on the installed area must consistently adhere to the dilatation joints already existing on the bedding, on the load-bearing structure and on the walls (main object joints).

It is necessary to adhere to the dilatation joints near the wall crossings, columns and other constructional parts passing through the floor (marginal joints). The product is installed in 1 cm distance from the walls, columns, breaks, corners, etc., the gap is bridged by a socle and filled with elastic binder.

In the case of large areas the dividing joints are created by dividing the area according to the following manner:

squares of approximately 4x4 m for installation on a surface exposed to high traffic, mechanical, dynamical or thermal load and on the beddings subject to motions or flexures.

squares of approximately 7x7 m on stable areas

The dilatation joint should have a rectangular cross-section with the side ratio 2 : 1.

The dilatation joint can be created by using the original dilatation strips or the Mapei system with elastic filling.

The elastic filling is built by using an elastic sealing gasket (rope) MAPEFOAM, which is pushed into the joint. The width of the rope is chosen greater than the width of the joint (1 cm wide joint – rope with the diameter of 1,5 cm). The upper part of the joint is filled according to the requirements for the traffic on the floor with the jointing silicone binder MAPESIL AC (standard traffic) or MAPEFLEX PU21 (heavy traffic, horizontal floor) or MAPEFLEX PU30 (heavy traffic, slanted floor). Before the binders are applied the edges of the dilatation are impregnated by the PRIMER FD agent.

The dilatation joints must be secured by the edge-protecting profiles in the case of dynamic loading (travelling of vehicles), in the case of increased dynamic loading protecting metal profiles are recommended, which have the shape of transitional bridge, that covers the joint.

Unsawn full-format tiles must be installed along the working and dividing joints; cut sizes implied by the field dimensions must be installed inside the fields.

## Jointing

During the preparation and application of the jointing materials it is necessary to follow the instructions of their producers.

The tiles should be installed with adherence to the joint size from 3 up to 10 mm according to the characteristics of the bedding, the dimensions, dimensional stability and thermal expansion coefficient of the product and according to the environment, where the installation takes place.

In the case of small areas without a high mechanical or thermal load the width of the joint is chosen 3 – 6 mm.

In the case of large areas, larger formats or higher mechanical or thermal load the width of the joint is chosen 5 – 10 mm and the joint after each 5th – 6th tile is jointed by a silicone jointing material.

First the jointing of dilatation joints and of the joints done with silicone binder is carried out. Jointing with cementing jointing materials is done after 24 hours.

The cementing jointing materials are always spread over the whole tile. After the setting of the material in the joint starts (never earlier!), the surface of the joint is prepared (smoothed) with a moistened sponge and the remains of the jointing material are rubbed down from the tiles. The final cleaning of the surface by using recommended cleaning agents is done after the setting of the material in the joints is finished, not earlier than after 24 hours.

The jointing materials listed in the section 6.2.2 are used for jointing.

The jointing material KERAPOXY is recommended for workshops with chemical load.

It is necessary to wait before the start of the jointing:

24 hours in the case, when the adhesive KERALASTIC is applied during the installation (at the temperature 23°C)

at least 4 hours in the case of the adhesive ELASTORAPID or GRANIRAPID (at the temperature 23°C).

### Cleaning of the floor tiles after finished jointing

After the setting of the material in the joint starts (never earlier!), the surface of the joint is prepared (smoothed) with a moistened sponge and the remains of the jointing material are rubbed down from the tiles. Especially the thicker deposits of the jointing material are removed from the surface. The redundant deposits of the material on the margins of joints, that would be difficult to wash out after the setting is finished, are removed by smoothing the material in the joints.

The final cleaning of the surface is done by using recommended cleaning agents after the setting of the material in the joints is finished, not earlier than after 24 hours.

The recommended cleaning agents listed in the section 7.3 are used for cleaning. It is necessary to follow the instructions given in the section 7.2.

It is necessary to realise that the surface of a product made from the engineered stone, especially with the polished finish, is more sensitive to the erosion of surface that is exposed to strong chemicals or exposed to chemicals for a long time, than a natural granite or hardened ceramics. These chemicals are also contained in the used surface cleaning agents. Therefore the exposure to cleaning agents, especially the strong ones used at increased amount of impurities, has to be limited to a time period necessary to remove the impurity, which duration is in the order of minutes! After that time it is necessary to remove the cleaning agent together with the released remains of the jointing material and of the impurities from the surface, preferably by evacuating them, and immediately wash the surface carefully.

This is the only way to clean the surface of the product without causing any damage to it.

## Installation of floor tiles on surface with floor heating

In these cases, it is necessary to pay special attention to the quality of substrate concrete and to take into account the thermal expansion of the product. It is recommended to use the cement finish Topcem for producing the bedding, for further reading see sections:6.3.1, 6.3.5. Before the installation is started, it is necessary to switch the floor heating on, in order to achieve a complete drying-up and stabilization of the bedding. After it is warmed up (dried-up and stabilized), the floor heating is switched off. After the bedding is cooled down to its original temperature it is possible to start the installation. It is necessary to bear in mind the higher count of dilatation and dividing joints. For gluing it is necessary to use the adhesive binder Elastorapid from the Mapei company.

## Installation of the product at higher thermal load

Valid for e.g. the installations around fireplaces, stoves, on strongly insolated areas (shop windows)….

In such cases it is necessary to pay special attention to the quality of the substrate concrete and take into consideration the thermal expansion of the product. It is recommended to use the cement finish Topcem for producing the bedding, for further reading see sections:6.3.1, 6.3.5. As the adhesive binder is in the case of high load recommended the binder Karalastic, in the case of low or medium load the binder Elastorapid. The adhesive binder Kerapoxy is recommended for usage in the case of concurrent thermal and mechanical load (strongly insolated travelling areas). Higher number of dilatation and dividing joints is to be taken into account.

## Installation of the product as stair component

During the installation the mechanico-physical characteristics of the product have to be taken into account (flexure strength, thermal expansion …). The wall junction must enable longitudinal changes of the stair component, i.e. the space on the interface between the wall and the component must be filled with an elastic material, which enables dilatation.

In case of gluing to concrete, the substrate layer has to be made from quality and mature concrete. For gluing it is necessary to use the adhesive binder Elastorapid from the Mapei company.

In case of gluing to metal constructions it is necessary to use quality elastic-stable organic based adhesive binders, e.g. the binder Keralastic from the Mapei company.

## Installation of glued wall tiles

The weight of the tiles from a Technistone product and its mechanico-physical characteristics, especially the thermal expansion, have to be taken into account during the installation of the glued cladding.

It is recommended to install the tiles of the total height greater than 2.5 m above the level of solid bedding by means of anchored or grate systems.

During the preparation and usage of the bedding and adhesives the above-mentioned principles are to be followed.

During the application of the adhesives it is possible to use the system of double-coating, see section 6.7.

It is necessary to apply a bonding primer to the bedding (e.g. Primer G from Mapei company, to starved bedding), and other types of penetration according to the absorption capacity of the bedding. New beddings must be properly matured.

The gluing can be performed by using the adhesive binder Elastorapid from the Mapei company.

Installation of formats is done individually. The formats are pressed carefully into their required positions; segments placed between the corners can determine the joints.

The installation of the formats starts at the floor plane and if this base is not horizontal, then from a lath batten, which temporarily replaces a solid tier. During the installation the horizontal and vertical flatness is to be checked.

After the adhesive is dried-up, the possible wooden lath, which replaced the first tier of tiles, is removed and the mounting of the remaining tier is done.

The joints are filled with a suitable jointing material. The silicone binder Mapesil AC is recommended, by using a rubber or plastic spatula.

Afterwards, the installed cladding is first cleaned by a wet sponge and then careful cleaning is carried out by means of recommended cleaning agents.

In case of need contact a producer representative or the technical service of the Mapei company.

# Maintenance and cleaning of the Technistone product

## General information about maintenance and cleaning

Resistance of the Technistone product surface to mechanical and chemical influences is given by the raw materials used (silicates, hardened polyester resin). The hardness of the surface (6 – 7 grade according to Mohs), compactibility and a very low absorbability make the product highly resistant to common influences. Even so, the protection of the product surface under a long-term exposure to abrasive impurities (this holds mainly for a product installed on the floors) is the reason for recommending the regular maintenance and cleaning of the product surface. This ensures the stability of the surface finish and of the aesthetic appearance of the product.

A product applied e.g. for kitchen countertops does not require a special maintenance and is maintained by usual non-abrasive kitchen cleaning agents. Nevertheless, cleaning and curing agents for the surface are mentioned also for such product applications here. These agents make the maintenance of the surface at common kitchen operation, e.g. at long-term and regular contact with the drops of oils spurted at frying or with the drying drops of dirty water, significantly easier.

The cleaning and maintenance of the engineered stone Technistone depends on the sort of surface finish of the product, on the location of the product, on the mechanical load of the product, etc. For cleaning and maintenance, especially of larger surfaces, it is recommended to order specialized company experienced in maintenance of the Technistone products or engineered stone.

## Important instructions for cleaning the products

Before using chosen cleaning or protecting agent (especially valid for industrial cleaning agents for the cleaning of floors), it is necessary to test it on a small area and not until after the evaluation of the results on a dried-up product carry out the overall application!!

Most of the agents are to be diluted according to the instructions from the producer!!

After using cleaning agents it is always necessary to remove the cleaning agent and the released impurities from the product surface quickly and carefully and to wash the surface thoroughly with pure water!!

Longer and not necessarily required exposure to aggressive cleaning agents will probably erode the product surface!!

The product surface (especially its polished surface finish) does not resist in the long-term to exposure to strong alkalies (NaOH, KOH...) and does not resist even in the short-term to the fluorhydric acid (HF). These chemicals are contained in some cleaning agents, which are available on the market. Therefore, for cleaning the surfaces it is important to use only products, which are suited for the cleaning of engineered stone; they may not be identical to the cleaning agents for natural granites or ceramics.

For cleaning, especially after the installation and jointing of floor tiles or for the cleaning of the tiles, which are highly dirty in the long term, use recommended products and not the mixtures of chemicals (lye, muriatic acid, hypochlorite...). For cleaning and maintenance, especially of larger surfaces, it is recommended to order specialized company experienced in maintenance of the Technistone products or engineered stone.

It is necessary to take into account and be in compliance with the recommendations of the producers pertaining to the usage (e.g. dilution...) and with the safety regulations of used agents. It is necessary to use protecting instruments according to the instructions from the producer.

Also the undermentioned facts, based on experiments and practical experience, are to be assessed and taken into consideration. Only general instructions are provided here, because the producer of the engineered stone has no influence on the individual conditions of performing the maintenance.

## Recommended special agents

For cleaning and maintenance the products from the companies Bellinzoni, Möller Chemie, Industrial Chem Italia and Akemi are recommended. The companies offer integral product ranges for these purposes.

| Firm: Bellinzoni | Contact: www.bellinzoni.com |
| --- | --- |
| Type | Product | Usage | Note |
| Cleaning | LEM 3 | standard cleaner | possible to dilute |
|  | BERT 27 | extra strong acid cleaner, limited exposure time!! | necessary to dilute!! |
|  | K 3 | extra strong alkali cleaner, limited exposure time!! | necessary to dilute!! |
|  | DECER DOS | wax washing | possible to dilute |
|  | ULTRA STRIPPER | strong washing of fat, waxes and oils... | necessary to dilute!! |
|  | MANGIA MACCHIA | stain remover | - |
|  | HYGIENIX | disinfection | necessary to dilute!! |
|  | WALL CLEAN | graffiti remover | - |
|  | ALGA KILL | remover of algae, mosses and mildew | possible to dilute |
| Surface protection, gloss enhancement | RR / 1 | waxing of floors | necessary to dilute |
|  | AS 11 | waxing of floors with anti-slip | necessary to dilute |
|  | MYTHOS | waxing of heavily stressed floors | necessary to dilute |
| Surface protection, impregnation | ANTIGRAFFITI S.V | protection against graffiti | - |
|  | BLOCK D 70 | protection against fat | possible to dilute |
|  | VIEUX | protection against impurities, color highlighting | necessary to dilute |
|  | KER 13D | impregnation against liquid impurities | - |
|  | POROSIL | Impregnation | - |
|  | IDEA XC | impregnation against liquid impurities | - |
| Regular maintenance | L&L | concurrent washing and waxing | necessary to dilute |
|  | AS 22 | concurrent washing and waxing with anti-slip | necessary to dilute |

| Firm: HMK Möller-Chemie | Contact: www.moeller-chemie.de |
| --- | --- |
| Type | Product | Usage | Note |
| Cleaning | R 55 | basic cleaner | possible to dilute |
|  | R 63 | extra strong acid cleaner, limited exposure time!! | necessary to dilute!! |
|  | R 75 | extra strong cleaner, rust remover, limited exposure time!! | necessary to dilute!! |
|  | R 77 | rust remover, limited exposure time!! | necessary to dilute!! |
|  | R 54 | washing of fat, waxes... | - |
|  | R 60 | remover of algae, mosses and mildew | necessary to dilute!! |
| Surface protection, impregnation | S 31 | impregnation against liquid impurities | - |
| Regular maintenance | P 24 | basic washing | necessary to dilute |

| Firm: AKEMI | Contact: www.akemi.de |
| --- | --- |
| Type | Product | Usage | Note |
| Cleaning | Stone cleaner | quick alkali cleaner, limited exposure time!! | necessary to dilute!! |
|  | Remover of cement deposits | strong acid cleaner, limited exposure time!! | necessary to dilute!! |
|  | Rust remover | rust removal, cleaning, limited exposure time!! | necessary to dilute!! |
|  | Wax remover | removing of waxes and fat | necessary to dilute |
| Regular maintenance | Soap for stone | concurrent basic washing and protection | necessary to dilute |

| Firm: Industrial Chem Italia | Contact: www.industrialchem-italia.com |
| --- | --- |
| Type | Product | Usage | Note |
| Surface protection, impregnation | NEW MICROKEM DC8 | impregnation against impurities, gloss enhancement | - |
|  | GREEP | agent increasing antislipperness properties of polished surfaces | possible to dilute |
|  | ANTISLIP K37 | agent for building antislipperness strips | - |

## Recommended equipment for mechanical curing of the product on floors

one-disk floor washer with 200 – 300 rpm (for all operations)

water vacuum cleaner, or water extractor

nylon pads with boar’s hair (for washing), white PAD LUX (for applying and pulling-over)

microfilament mop for applying and spreading waxes and impregnations in aluminium construction

## Cleaning of the product surface

### Cleaning of the surface after installation or before the application of protecting wax / impregnation layer

An appropriate cleaner is applied to the surface of the product (best done by machine, always with PAD disks). After its action (only for the shortest necessary period) is the cleaner together with the released impurity carefully removed (in the best case by a machine called water extractor, where rinsing of the impurities under pressure and their evacuation are taking place at the same time). Consequently, it is recommended to wash the product surface with pure water.

In case of a low contamination the cleaners LEM 3 or R 55 are recommended, at strong contamination the agents BERT 27, K 3, R 63 or the Remover of cement deposits. When the surface is contaminated by oil, the fat remover DECER DOS, Ultra Stripper or R 54 is used first.

### Cleaning of the product in households (kitchen countertops, tables..)

The product used in households does not require a special protection, it is sufficient to wipe it with warm water or to use usual household non-abrasive agents. In case of need to clean intensely (e.g. removing old fats around a boiling plate, boiling incrustation at the flush basin...) it is possible to use the above mentioned agents as e.g.:. Ultra Stripper, DECER DOS, LEM 3 or R 55.

### Special cleaning of the product surface

Rust: agents R 75, Rust remover.

Thick (fat) stains: agents Ultra Stripper, Mangia Macchia

Disinfection: agent Hygienix, further e.g. the agents of the companies Bochemie (www.bochemie.cz) and Farmak (www.farmak.cz).

Moss, mildew, algae: Agents Alga Kill, R 60, further e.g. the agents of the companies Bochemie, Farmak, Agrochem.

Graffiti: agents Wall Clean, (final cleaning Ultra Stripper)

After using these agents it is recommended to wash the product surface subsequently with soap and pure water.

## Protection of the product with polished surface

Protecting and impregnating agents are always applied to a clean and dry surface

Protecting and impregnating agents are applied and spread by a microfilament mop. Excessive agent is wiped away. After the protecting or impregnating coating is dry, it is pulled-over. When pulling-over is done by a machine it is always necessary to use only the disks with artificial fibres (PAD LUX) and not disks with steel wires!

During application it is possible to apply the waxes subsequently in several layers (up to three), always after drying-up, perpendicularly to the preceding layer. It is necessary to leave a pause of at least 24 hours between the application of waxes of various types.

Washing of the floor tiles is not possible earlier than after 24 hours from the wax application.

### Protection of the product surface on floors with low mechanical and abrasive load

These surfaces are to be cured regularly (with a 0.5 – 2 years period according to the traffic level) with the RR / 1 or AS 11 wax by using a machine. In the case of heavier traffic it is possible to provide basic protection by the application of the Mythos wax and possibly by subsequent application of the RR / 1 and AS 11 waxes (the application of different waxes is to be separated by at least 24 hours delay).

### Protection of the product surface on floors with higher mechanical and abrasive load

These surfaces are to be cured regularly (with a 0.5 – 1 year period according to the traffic level) with the Mythos wax with possible subsequent application of the RR / 1 or AS 11 waxes by using a machine (the application of different waxes is to be separated by at least 24 hours delay).

### Improvement of surface antislipperness finish

For increasing sliding friction of a polished surface it is possible to apply the Greep agent to the basic wax layer or to use the AS 11 agent as the basic wax. These agents increase sliding friction, but they do not replace a coarser surface finish intended for achieving slip-resistance defined in relevant standards.

Distinctive slip-resistance, e.g. at the end of the step-on surface on stairs, can be achieved by creating an antislipperness strip by means of the application of the Antislip K 37 agent.

### Regular maintenance of the floor areas with polished surface

It is possible to wash the floor tiles after at least 24 hours since the wax application.

It is very advantageous to use special agents for everyday regular surface washing, because they combine the washing effect with the spread of thin protective wax layer, which prevents progressive removal of the basic protective layer and prolongs its durability substantially. The agents L&L, AS 22 are recommended (with anti-skid effect). The agents Soap for stone or P24 can be used, too. In this case the usual washing is done without any use of detergents.

On no account acids, strong alkalies or detergents containing fat are used for washing.

## Protection of product with semi-gloss, honed surface

It is recommended to provide protection of the products with such surface finishes by means of impregnation agents, Porosil, Idea XC, Ker 13D, S 31, New Microkem DC 8, (Vieux – smaller areas). By using these agents a water-repellent layer is created on the product surface, which prevents intrusion of impurities into the coarser parts of surface layer.

Protective and impregnation agents are always applied and spread on a clean and dry surface by a microfilament mop. Excessive agent is wiped away. After drying-up the protective and impregnation layer is pulled-over.

When application and spreading is done by a machine it is always necessary to use exclusively the disks with artificial fibres (PAD LUX) and not disks with steel wires!

According to the degree of surface load it is necessary to renew the impregnation after some time.

## Protection of brushed/antique finish or blasted product surface

For protection of a product with such surface finish the impregnation agents, New Microkem DC 8, Idea XC, Ker 13D, S 31 are recommended. By using these agents a water-repellent layer is created on the product surface, which prevents intrusion of impurities into the coarser parts of surface layer and highlights the color shade of the product.

Impregnation agents are always applied and spread on a clean and dry surface by a microfilament mop. Excessive agent is wiped away. After drying-up the impregnation layer is pulled-over.

When spreading is done by a machine it is always necessary to use only the disks with artificial fibres (PAD LUX) and not disks with steel wires! Only inevitable amount of the impregnation agent is applied, the excessive amount of the agent is to be removed from the product surface.

According to the degree of surface load it is necessary to renew the impregnation after some time.

### Regular maintenance of floor areas with honed, brushed/antique finish and blasted surface

It is possible to wash the floor tiles after at least 24 hours since the impregnation application.

Washing of an impregnated surface is done only with lukewarm water. In case of greater contamination 1 spoon of LEM (Bellinzoni) agent is added to a pail of water. So, the usual washing is done in this case without any usage of detergents.

On no account acids, strong alkalies or detergents containing fat are used for washing.

According to the degree of surface load it is recommended to renew impregnation regularly.

## Protection of surface of furniture components, kitchen countertops, wall cladding

The product used in households and on interior wall cladding does not require a special protection, it is sufficient to wipe it with warm water or to use usual household non-abrasive agents. When the surface has to be more water-repellent or oil-repellent (especially on kitchen furniture) it is possible to use the impregnation agents Block D 70, New Microkem DC 8, Porosil, Idea XC. These agents build a film on the surface of the product, which makes it harder for impurities to stick to the surface (e.g. oil drops from frying) and makes usual cleaning easier. These agents are applied and pulled-over manually by a soft rag, or possibly by using a manual polishing equipment (e.g. manual eccentric grinder with mounted polishing disc). Before that the surface must be cleared from mechanical impurities, dust and it must be washed.

## Protection of surface against paints and varnishes

To protect the surface against paints (graffiti) it is possible to use the protective agent Antigraffity S. V. The paints can be easily removed from a protected surface by polishing disc or by vapour. The surface protection is also increased by the impregnation agents mentioned above. To remove paints and varnishes from an unprotected surface it is possible to use the agent Wall Clean and for final treatment the Ultra Stripper agent.

## Protection against abrasive mechanical impurities

When higher mechanical load of the product combined with greater abundance of abrasive and liquid contaminants is expected it is recommended to install a cleaning zone (brushes) in front of the surface. Especially in winter season, this zone collects a great part of impurities and in this way protects the product surface and prevents quick decrease of the protective wax layer. It is recommended to install the cleaning zones especially in shops, offices, halls, corridors with the entrance directly from the street.

## Renewal of floor tiles (polished surface)

In case of damage (gloss loss) of the surface of floor tiles it is possible to renew the surface by re-honing. The gloss of the surface is increased, but deep defects are not remedied. This operation can be carried out only by experienced, specialized companies with appropriate equipment. It is always necessary first to test the renewal, possibly on a small, unexposed surface.

After the surface of floor tiles is washed the renewal of gloss is done by the polishing powder Bellinzoni KP 85 (Klindex / marble variant). Approximately one tablespoon of the powder is sprinkled onto the floor tiles and a small amount of water is poured onto it, in order to create a diluted material, which is polished by a one-disc floor machine with nylon pad Discolux for a period of 8 – 10 min. This amount is sufficient for the renewal of about 3 – 5 m2 of the surface. Then the surface is washed with pure water, which is evacuated. To achieve the desired outcome it is appropriate to repeat the procedure two times. After the final thorough wash is finished it is possible to start the application of the protective wax, see section: 7.6.

# Other machining of the product

## Binding and gluing of the product

For binding and gluing of the product it is recommended to use the binders and adhesives from the companies Bellinzoni (Astra 24 K, Mastice 2000, Blitz, Expo 2000), Akemi, Möller Chemie during further machining in stonework shops. These products are based on polyester, acrylate and epoxide resins. There are transparent, polishable, filled or unfilled with a filler, trickling, non-trickling, frost resisting binders and adhesives available, it is also possible to use tinters for binder dying.

It is possible to use also commercial two-part epoxide or polyester adhesives of silicone binders.

## Cutting and milling of the product

In fabrication shops, the product is cut, milled and worked the same way and using the same equipment as for natural granite. For cutting, diamond discs and water-cooling are used.

## Drilling of the product

In fabrication shops, the product is drilled the same way and using the same equipment as for natural granite. To drill bigger diameters, diamond drills and water-cooling are used. Smaller diameters can be drilled with widia drills without impact.

## Honing and polishing of the product

In fabrication shops, the product is honed and polished the same way and using the same equipment as for natural granite. It is necessary to use complete sets of abrasives, so that there are not visible marks from previous machining.

# Answers to frequent questions of the customers

## What is it Technistone® ?

Technistone® is a compact, hard, imporous, composite product supplied in the form of slabs, formats (tiles), or mosaics with a wide range of applications in private, public and industrial sector as a component of kitchen, bathroom and table countertops, parapets, floor tiles, wall cladding, mosaics, etc.. Taking into account the used raw materials and production technology, Technistone® achieves excellent properties due to its strength and compactibility. The wide range of color shades, surface finishes, thicknesses and dimensions enables always to choose a suitable combination conforming to both esthetical and qualitative requirements.

## What is Technistone® made from?

Technistone® is produced from high-quality natural raw materials (quartzes, granites), mirror and glass granulates, from a small amount of color pigments and quality polyester resin. More than 90% of the product mass is formed by natural components, therefore, the content of the polyester resin is less than 10%.

## Is Technistone® the same throughout its volume or is its color and structure built only on the surface?

Technistone® has homogeneous structure and color throughout its volume. Both, the front and back faces of the product can be machined and polished, any holes and grooves can be milled, edges can be treated. The shade and the structure will be identical.

## What is the comparison of Technistone® (used e.g. on a kitchen countertop) to natural granite, marble, Corian® or postforming?

Technistone® has in comparison to natural granites greater flexure strength, at the same thickness is more resistant against e.g. impact and load. With the Technistone® products (especially of the Granite range) you will get the feeling of solid granite, but with multiple times lower absorbability of the surface, which does not absorb food and drinks. Technistone® is harder and more resistant than natural marble. Moreover, it is composed mainly of silicates, which are acidproof as opposed to marble.

Technistone®, as opposed to the Corian® or postforming products contains more than 90 % of anorganic materials. The Technistone® surface is in virtue of that far more hard, resistant and durable.

## How can the individual types of Technistone® be characterized?

Technistone® is offered in four lines of products (production groups), which differ from each other by the used raw materials and consequently also by their appearance and some properties. Brief characteristics of individual lines follow.

SAND (commercial name Gobi)

These products are made from sorted siliceous sands. The most significant characteristic is the fine texture of the surface.

Advantage: The highest reached strength, high resistance of the surface and uniform appearance.

GRANITE (commercial names Taurus, Karpat, Kalahari, Sonora)

Through the combination of attractive natural granites and siliceous sands a characteristic „granite“ texture of the surface is created, which is tuned with the overall color shades of the products.

Advantage: Natural appearance combined with strength and practical non-absorbability of the surface, which is not found at natural granites.

MIRRORS (commercial name Starlight)

High-gloss surface of the product with luminous mirror effects built from compact mirror granulates.

Advantage: Completely untraditional appearance makes it possible to combine the product with high-end image and with classical materials.

CRYSTAL (commercial name Crystal)

The product is made from one of the hardest minerals – the translucent or milky natural, sorted quartz imported from the top-quality world collecting localities.

Advantage: Combination of strength, beauty and purity.

A new product line called Venetian line is under preparation.

## Resists the Technistone® surface used on the kitchen countertop mechanical damage?

The Technistone® product is manufactured from hard minerals and achieves high strength, which predetermines it to a very successful application as kitchen countertops. Usual cutting or beating of meat with a wooden meat beater directly on its surface causes no problems to the product.

Each composite product, no matter how resistant, can of course be damaged by strong, concentrated pressure or by heavy impact, e.g. by strong pressure on the tip of a knife or by a strong hit of a metal mallet. Technistone® belongs to the most resistant products used for kitchen countertops, nevertheless, it is not completely undamagable.

## Resists the surface of the Technistone® product used on the kitchen countertop thermal load?

As opposed to the kitchen countertops from postforming or Corian® the Technistone®, thanks to the used raw materials, is resistant to thermal loads occurring in kitchens. Technistone® is also practically inflammable, it is not set on fire by a burning matchbox or ignited oil.

The heat-shock resistance is increased with the increase of the used thickness of Technistone®, a slab with the thickness of 30 mm is far more resistant than a 10 mm slab. Sudden and short putting aside of a pan with oil or a pot with boiling water will probably not cause damage to the surface of a 20 and 30 mm countertop, if the hot object is not put aside near the edge or a cut-out of the desk and is returned back after a short while. In spite of this resistance, the Technistone® surface, like any other composite material, may be damaged by a sudden or lasting exposition to high temperatures (over 100 °C), mainly at the edges and cut-outs of the product, where a crack may appear. Therefore, it is necessary to use insulating pads for putting hot objects aside. These pads must also be placed below every electrical cooking and baking appliances located on the kitchen countertop.

## Is the Technistone® product harmless to health?

The product is certified by the National health institute for health harmlessness, the certificate declares the suitability of using Technistone® for the production of kitchen countertops.

The product is certified by the NSF International organization with this outcome: the product complies with the Standard 51 NSF/ANSI – Food equipment materials, Solid surfaces for Splash zone.

## Are the chromatic and structural particles taking their part at the appearance of the Technistone® surface intentional?

Technistone® is mainly built from several chromatic components and granulates of different sizes, which determine its characteristic color structure. These components, which are inevitably created during the production process are from a greater part mixed together and from a smaller part they remain in the original form, in order to achieve the characteristic appearance of Technistone®. For this reason, varicolored parts, as well as structural elements of various sizes are always visible on the product surface.

## Is it necessary to take into account the thermal expansion when using the Technistone product as floor and wall tiles?

The polyester resin used as a binder causes not only the increase in the strength characteristics, but also in the thermal expansion of the product, which is higher than the thermal expansion of natural stone or ceramics. Therefore, it is necessary to take this fact into consideration during designing the floors and wall claddings from Technistone®.

# Safety regulations for the product

Identification

Product identification:   Engineered stone Technistone®

Manufacturer:   Technistone a.s.

Bří.Štefanů 1070

Hradec Králové

500 03

Czech Republic

Telephone number:   00420 495 714 711

Fax number:        00420 495 714 709

E-mail address:      info@Technistone.cz ,

Web site:           www.Technistone.com

Prepared by: Technistone a.s. – Technical department

Composition

| Components / Materials | % by weight | CAS Number |
| --- | --- | --- |
| Unsaturated polyester resin (cured during processing) | max 10 | --- |
| Silicates (silica sands, quartz’s, granites, glass, cristobalite) | max 94 | 100 14464 – 46 - 1 |

Exposure limits may be applicable for the following:

Silica crystalline (quartz).

Components (remarks)

Material is not known to contain Toxic chemicals under Section 313 of Title III of the Superfund Amendments and Reauthorization Act of 1986 and 40 CFR part 372. (Used in USA.)

Physical Data

| Physical state: | Solid |
| --- | --- |
| Color: | Varied |
| Appearance: | Varied (Monocolor, Multicolor, Granite, Mirror..) |
| Odour: | Odourless |
| Specific Gravity: | 2100 – 2600 kg / m3 |
| Boiling point: | Not applicable |
| Freezing point: | Not applicable |
| Miscibility: | Not applicable |
| % Volatiles | 0 % at room temperature |
| Fire Fighting Data |

## Flammable Properties

Engineered stone Technistone® can be combusted only with difficulty.

Thermal decomposition products resulting from polymer and pigments degrading at elevated temperatures include various hydrocarbons, carbon dioxide, carbon monoxides, soot and water. Fumes of metal oxides could be also released.

## Extinguishing Media

Water, dry chemical, CO2, foam.

## Fire Fighting Instruction

Keep personnel removed and upwind of fire. Wear self-contained breathing apparatus.

## Self Ignition Temperature

Ignition temperature reached out by hot air and flame influence: 445°C / 833°F

Ignition temperature reached out only by hot air influence: 550°C / 1022°F

Stability And Reactivity

Engineered stone Technistone® (silica based product) is chemically stable at normal temperatures and storage conditions.

| Polymerization: | Polymerization will not occur |
| --- | --- |
| Incompatibility with other substances: Results: | Sodium, potassium hydroxides Leaching of coloration |
| Reactivity with other substances: Results: | Hydrofluoric acid Material degradation |
| Hazardous decomposition products: | None |

Toxicological Properties Of The Made Product

| Product sensitization: | None |
| --- | --- |
| Product carcinogenity: | None |
| Product teratogenicity: | None |
| Product irritancy: | See section 10.11 |
| Inhalation of the dust generated during product handling: | See section 10.11 |

Hazardous Identification During Handling

### Potential Health Effects

Engineered stone Technistone® is not hazardous as shipped and used.

When the processes of sawing, routing, drilling, sanding and polishing are carried out as dry process, there is the greatest generation of airborne dust. When these operations are carried out with water for cooling, lubrication and dust depression, then the quantity of airborne dust is reduced by 90 – 98%. These reducing covers potential exposure to workers.

However, stone work operations such as sawing, routing, drilling, sanding and polishing can generate dust. High concentration of dust can irritate eyes, nose and respiratory passages and cause coughing and sneezing.

Dust generated during handling of engineered stone Technistone®, can contain particles of crystalline silica (quartz). Overexposure to airborne quartz can cause silicosis and chronic and progressively debilitating disease, characterized by the formation of silica-containing scar tissue in the lung. The risk of lung disease increases if smoking is combined with silica dust inhalation. Individual with pre-existing diseases of the lungs may increase susceptibility to the toxicity of excessive exposures.

### Personal Protective Equipment

Information is available in ASTM E 1132-89 Standard practice for health requirements relating to occupational to exposure quartz dust.

Observe local safe handling procedures.

| Eye, face protection: | Wear safety glasses during operations such sawing, sanding, drilling, honing or routing. |
| --- | --- |
| Respirators: | During sawing, sanding, drilling, honing, polishing or routing operation always use respirator with air purifying cartridge. Respirators are selected and used based on the form and concentration of the contaminant in the air. Avoid breathing dust! |
| Protective clothing: | Wear leather or cotton gloves when handling larger pieces and during operation such as sawing, routing or drilling. |
| Protective footwear: | Use steel toed footwear when handling larger pieces. |

### Procedures And Controls

Information is available in ASTM E 1132-89 Standard practice for health requirements relating to occupational to exposure quartz dust.

Observe local safe handling procedures. Handle with care.

| Engineering controls: | Use ventilation and water cooled tooling and equipment that is adequate to keep employee exposure to airborne concentrations below recommended limits. Provide for appropriate exhaust ventilation and dust collection at machinery. |
| --- | --- |
| Storage requirements: | No special requirements, should be stored in dry, clean place without oil or other contaminants. |
| Shipping requirements: | Appropriate banding material has to be used. |
| Waste disposal procedures: | Observe local regulations for disposal. |

### First Aid Procedures

Inhalation

If larger amounts of dust are inhaled, remove to fresh air. If breathing becomes difficult, seek medical assistance immediately.

Eye contact

In case of eye contact, flush eyes with plenty of water for at least 15 minutes. Consult a physician.

Skin contact

The compound is not likely to be hazardous, but flushing of the skin with soap and water is advisable.

Ingestion

Consult a physician.

Ecological Information

No ecological information is available.

Disposal Consideration

Product disposal: Dispose of in accordance with state and local regulations.

Other Information

Disclaimer Notice

The data in this Material Safety data Sheet relates only to the specific material designated herein and does not relate to use in combination with any other material and in any process.

# Records

# Related documents

## Internal

VP 03-03 –Claim rules in the organization

VP 04-06 –Storage management of products of mass production

VP 04-03 –Planning and process of main production

VP 04-10 –Technical standard for engineered stone

VP 04-11 – Quality indicators and classes

VP 04-13 –- Technical standard for products from fabrication shop

VP 04-14 –- Planning and process of production in fabrication shop

VP 09-13 – Claims procedure

PS 04-07-03 –Interoperational technological control at the production of the semi-finished

products

PS 04-07-04 – Technological control at the production of the final product

PS 04-07-06 – Control of the final product and its labelling

## External

ISO 9001:2000 – Quality management systems – Requirements

ISO 9000:2000 – Quality management systems – Foundations, principles and terminology

Technical standards and specifications mentioned in the text